|  | Reference | d̄ | D | dmax | RBC | ρd | σ3 | qf |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Tu (2017) | 1.227 | 300 | 60 | 0.0 | 1.900 | 100 | 233.2 |
| 2 |  | 1.227 | 300 | 60 | 0.0 | 1.900 | 200 | 485.5 |
| 3 |  | 1.227 | 300 | 60 | 0.0 | 1.900 | 400 | 898.3 |
| 4 |  | 1.227 | 300 | 60 | 0.0 | 1.900 | 600 | 1234.7 |
| 5 |  | 1.227 | 300 | 60 | 0.0 | 1.900 | 800 | 1513.8 |
| 6 |  | 1.227 | 300 | 60 | 0.0 | 1.900 | 1200 | 2228.6 |
| 7 |  | 2.197 | 300 | 60 | 20.0 | 1.900 | 100 | 262.7 |
| 8 |  | 2.197 | 300 | 60 | 20.0 | 1.900 | 200 | 497.7 |
| 9 |  | 2.197 | 300 | 60 | 20.0 | 1.900 | 400 | 917.1 |
| 10 |  | 2.197 | 300 | 60 | 20.0 | 1.900 | 600 | 1248.9 |
| 11 |  | 2.197 | 300 | 60 | 20.0 | 1.900 | 800 | 1589.9 |
| 12 |  | 2.197 | 300 | 60 | 20.0 | 1.900 | 1200 | 2520.7 |
| 13 |  | 3.964 | 300 | 60 | 40.0 | 1.900 | 100 | 346.1 |
| 14 |  | 3.964 | 300 | 60 | 40.0 | 1.900 | 200 | 628.8 |
| 15 |  | 3.964 | 300 | 60 | 40.0 | 1.900 | 400 | 1077.3 |
| 16 |  | 3.964 | 300 | 60 | 40.0 | 1.900 | 600 | 1540.4 |
| 17 |  | 3.964 | 300 | 60 | 40.0 | 1.900 | 800 | 1988.9 |
| 18 |  | 3.964 | 300 | 60 | 40.0 | 1.900 | 1200 | 2900.4 |
| 19 |  | 7.026 | 300 | 60 | 59.0 | 1.900 | 100 | 370.6 |
| 20 |  | 7.026 | 300 | 60 | 59.0 | 1.900 | 200 | 669.1 |
| 21 |  | 7.026 | 300 | 60 | 59.0 | 1.900 | 400 | 1235.3 |
| 22 |  | 7.026 | 300 | 60 | 59.0 | 1.900 | 600 | 1739.7 |
| 23 |  | 7.026 | 300 | 60 | 59.0 | 1.900 | 800 | 2280.2 |
| 24 |  | 7.026 | 300 | 60 | 59.0 | 1.900 | 1200 | 3299.3 |
| 25 |  | 12.722 | 300 | 60 | 80.0 | 1.900 | 100 | 589.9 |
| 26 |  | 12.722 | 300 | 60 | 80.0 | 1.900 | 200 | 1023.8 |
| 27 |  | 12.722 | 300 | 60 | 80.0 | 1.900 | 400 | 1800.4 |
| 28 |  | 12.722 | 300 | 60 | 80.0 | 1.900 | 600 | 2561.1 |
| 29 |  | 12.722 | 300 | 60 | 80.0 | 1.900 | 800 | 3226.5 |
| 30 |  | 12.722 | 300 | 60 | 80.0 | 1.900 | 1200 | 4626.2 |
| 31 |  | 22.580 | 300 | 60 | 100.0 | 1.900 | 100 | 669.1 |
| 32 |  | 22.580 | 300 | 60 | 100.0 | 1.900 | 200 | 1146.2 |
| 33 |  | 22.580 | 300 | 60 | 100.0 | 1.900 | 400 | 2017.2 |
| 34 |  | 22.580 | 300 | 60 | 100.0 | 1.900 | 600 | 2849.7 |
| 35 |  | 22.580 | 300 | 60 | 100.0 | 1.900 | 800 | 3603.9 |
| 36 |  | 22.580 | 300 | 60 | 100.0 | 1.900 | 1200 | 5179.3 |
| 37 | Li et al. (2023) | 5.438 | 300 | 60 | 56.5 | 2.050 | 300 | 713.3 |
| 38 |  | 5.438 | 300 | 60 | 56.5 | 2.050 | 600 | 1272.7 |
| 39 |  | 5.438 | 300 | 60 | 56.5 | 2.050 | 900 | 1825.2 |
| 40 | Zhang et al. (2023) | 10.971 | 300 | 80 | 71.6 | 2.280 | 200 | 1142.9 |
| 41 |  | 10.971 | 300 | 80 | 71.6 | 2.280 | 400 | 1854.6 |
| 42 |  | 10.971 | 300 | 80 | 71.6 | 2.280 | 800 | 3378.5 |
| 43 |  | 6.878 | 300 | 80 | 59.7 | 2.290 | 200 | 1203.0 |
| 44 |  | 6.878 | 300 | 80 | 59.7 | 2.290 | 400 | 2115.3 |
| 45 |  | 6.878 | 300 | 80 | 59.7 | 2.290 | 800 | 3418.6 |
| 46 | Ding (2023) | 7.116 | 300 | 60 | 20.0 | 1.740 | 500 | 1398.4 |
| 47 |  | 7.116 | 300 | 60 | 20.0 | 1.740 | 1000 | 2273.4 |
| 48 |  | 7.116 | 300 | 60 | 20.0 | 1.740 | 1500 | 3218.8 |
| 49 |  | 7.116 | 300 | 60 | 20.0 | 1.740 | 2000 | 4203.1 |
| 50 |  | 10.126 | 300 | 60 | 30.0 | 1.870 | 500 | 1429.9 |
| 51 |  | 10.126 | 300 | 60 | 30.0 | 1.870 | 1000 | 2509.6 |
| 52 |  | 10.126 | 300 | 60 | 30.0 | 1.870 | 1500 | 3561.8 |
| 53 |  | 10.126 | 300 | 60 | 30.0 | 1.870 | 2000 | 4474.7 |
| 54 |  | 14.411 | 300 | 60 | 35.0 | 1.920 | 500 | 1435.6 |
| 55 |  | 14.411 | 300 | 60 | 35.0 | 1.920 | 1000 | 2613.8 |
| 56 |  | 14.411 | 300 | 60 | 35.0 | 1.920 | 1500 | 3596.9 |
| 57 |  | 14.411 | 300 | 60 | 35.0 | 1.920 | 2000 | 4603.4 |
| 58 |  | 20.509 | 300 | 60 | 40.0 | 1.960 | 500 | 1531.6 |
| 59 |  | 20.509 | 300 | 60 | 40.0 | 1.960 | 1000 | 2608.7 |
| 60 |  | 20.509 | 300 | 60 | 40.0 | 1.960 | 1500 | 3862.6 |
| 61 |  | 20.509 | 300 | 60 | 40.0 | 1.960 | 2000 | 4806.9 |
| 62 |  | 29.186 | 300 | 60 | 50.0 | 2.010 | 500 | 1545.8 |
| 63 |  | 29.186 | 300 | 60 | 50.0 | 2.010 | 1000 | 2795.5 |
| 64 |  | 29.186 | 300 | 60 | 50.0 | 2.010 | 1500 | 3917.1 |
| 65 |  | 29.186 | 300 | 60 | 50.0 | 2.010 | 2000 | 5005.8 |
| 66 | Lv et al. (2023) | 9.357 | 300 | 50 | 69.0 | 2.100 | 100 | 810.6 |
| 67 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 200 | 1360.3 |
| 68 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 400 | 2375.8 |
| 69 | Tao et al. (2022) | 9.357 | 300 | 50 | 69.0 | 2.100 | 100 | 585.2 |
| 70 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 200 | 960.8 |
| 71 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 400 | 1716.4 |
| 72 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 100 | 549.3 |
| 73 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 200 | 875.9 |
| 74 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 400 | 1706.2 |
| 75 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 100 | 559.2 |
| 76 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 200 | 855.6 |
| 77 |  | 9.357 | 300 | 50 | 69.0 | 2.100 | 400 | 1607.1 |
| 78 | Jin et al. (2017) | 12.621 | 300 | 60 | 82.0 | 2.176 | 100 | 493.4 |
| 79 |  | 12.621 | 300 | 60 | 82.0 | 2.176 | 200 | 1019.7 |
| 80 |  | 12.621 | 300 | 60 | 82.0 | 2.176 | 300 | 1144.7 |
| 81 | Fang (2023) | 5.101 | 300 | 60 | 55.5 | 1.760 | 100 | 479.7 |
| 82 |  | 5.101 | 300 | 60 | 55.5 | 1.760 | 200 | 787.6 |
| 83 |  | 5.101 | 300 | 60 | 55.5 | 1.760 | 400 | 1353.2 |
| 84 |  | 5.101 | 300 | 60 | 55.5 | 1.760 | 800 | 2334.1 |
| 85 |  | 5.101 | 300 | 60 | 55.5 | 1.820 | 100 | 538.3 |
| 86 |  | 5.101 | 300 | 60 | 55.5 | 1.820 | 200 | 899.3 |
| 87 |  | 5.101 | 300 | 60 | 55.5 | 1.820 | 400 | 1529.5 |
| 88 |  | 5.101 | 300 | 60 | 55.5 | 1.820 | 800 | 2619.3 |
| 89 |  | 5.101 | 300 | 60 | 55.5 | 2.000 | 100 | 820.1 |
| 90 |  | 5.101 | 300 | 60 | 55.5 | 2.000 | 200 | 1079.5 |
| 91 |  | 5.101 | 300 | 60 | 55.5 | 2.000 | 400 | 1774.1 |
| 92 |  | 5.101 | 300 | 60 | 55.5 | 2.000 | 800 | 3062.8 |
| 93 |  | 5.101 | 300 | 60 | 55.5 | 2.150 | 100 | 813.4 |
| 94 |  | 5.101 | 300 | 60 | 55.5 | 2.150 | 200 | 1138.8 |
| 95 |  | 5.101 | 300 | 60 | 55.5 | 2.150 | 400 | 1827.8 |
| 96 |  | 5.101 | 300 | 60 | 55.5 | 2.150 | 800 | 3177.0 |
| 97 |  | 5.101 | 300 | 60 | 55.5 | 2.300 | 100 | 971.8 |
| 98 |  | 5.101 | 300 | 60 | 55.5 | 2.300 | 200 | 1378.5 |
| 99 |  | 5.101 | 300 | 60 | 55.5 | 2.300 | 400 | 2101.7 |
| 100 |  | 5.101 | 300 | 60 | 55.5 | 2.300 | 800 | 3570.6 |
| 101 | Gao (2004) | 10.426 | 300 | 60 | 71.0 | 2.120 | 100 | 393.5 |
| 102 |  | 10.426 | 300 | 60 | 71.0 | 2.120 | 150 | 568.2 |
| 103 |  | 10.426 | 300 | 60 | 71.0 | 2.120 | 200 | 676.3 |
| 104 |  | 10.426 | 300 | 60 | 71.0 | 2.120 | 250 | 858.5 |
| 105 | Dong et al. (2021) | 8.282 | 300 | 60 | 30.0 | 1.770 | 200 | 420.2 |
| 106 |  | 8.282 | 300 | 60 | 30.0 | 1.770 | 300 | 536.3 |
| 107 |  | 8.282 | 300 | 60 | 30.0 | 1.770 | 400 | 664.6 |
| 108 |  | 8.282 | 300 | 60 | 30.0 | 1.890 | 200 | 400.0 |
| 109 |  | 8.282 | 300 | 60 | 30.0 | 1.890 | 300 | 511.8 |
| 110 |  | 8.282 | 300 | 60 | 30.0 | 1.890 | 400 | 667.2 |
| 111 |  | 8.282 | 300 | 60 | 30.0 | 2.020 | 200 | 423.8 |
| 112 |  | 8.282 | 300 | 60 | 30.0 | 2.020 | 300 | 554.5 |
| 113 |  | 8.282 | 300 | 60 | 30.0 | 2.020 | 400 | 718.8 |
| 114 |  | 8.203 | 300 | 60 | 30.0 | 1.770 | 200 | 376.9 |
| 115 |  | 8.203 | 300 | 60 | 30.0 | 1.770 | 300 | 567.1 |
| 116 |  | 8.203 | 300 | 60 | 30.0 | 1.770 | 400 | 666.7 |
| 117 |  | 8.203 | 300 | 60 | 30.0 | 1.890 | 200 | 425.1 |
| 118 |  | 8.203 | 300 | 60 | 30.0 | 1.890 | 300 | 638.6 |
| 119 |  | 8.203 | 300 | 60 | 30.0 | 1.890 | 400 | 748.0 |
| 120 |  | 8.203 | 300 | 60 | 30.0 | 2.020 | 200 | 432.0 |
| 121 |  | 8.203 | 300 | 60 | 30.0 | 2.020 | 300 | 627.6 |
| 122 |  | 8.203 | 300 | 60 | 30.0 | 2.020 | 400 | 734.2 |
| 123 |  | 8.188 | 300 | 60 | 30.0 | 1.770 | 200 | 386.9 |
| 124 |  | 8.188 | 300 | 60 | 30.0 | 1.770 | 300 | 526.9 |
| 125 |  | 8.188 | 300 | 60 | 30.0 | 1.770 | 400 | 616.2 |
| 126 |  | 8.188 | 300 | 60 | 30.0 | 1.890 | 200 | 436.8 |
| 127 |  | 8.188 | 300 | 60 | 30.0 | 1.890 | 300 | 596.5 |
| 128 |  | 8.188 | 300 | 60 | 30.0 | 1.890 | 400 | 668.4 |
| 129 |  | 8.188 | 300 | 60 | 30.0 | 2.020 | 200 | 412.3 |
| 130 |  | 8.188 | 300 | 60 | 30.0 | 2.020 | 300 | 557.9 |
| 131 |  | 8.188 | 300 | 60 | 30.0 | 2.020 | 400 | 635.1 |
| 132 | Huang et al. (2019) | 9.306 | 300 | 25 | 55.3 | 1.760 | 2000 | 4924.8 |
| 133 |  | 13.814 | 300 | 25 | 90.0 | 1.640 | 2000 | 4336.3 |
| 134 |  | 17.012 | 300 | 25 | 90.0 | 1.670 | 2000 | 4295.0 |
| 135 |  | 13.026 | 300 | 25 | 80.0 | 1.770 | 2000 | 4697.6 |
| 136 |  | 9.306 | 300 | 25 | 55.3 | 1.760 | 1000 | 2778.0 |
| 137 |  | 9.306 | 300 | 25 | 55.3 | 1.760 | 1500 | 3883.0 |
| 138 |  | 9.306 | 300 | 25 | 55.3 | 1.760 | 2400 | 5628.2 |
| 139 |  | 10.852 | 300 | 60 | 70.0 | 2.010 | 100 | 641.0 |
| 140 |  | 10.852 | 300 | 60 | 70.0 | 2.010 | 200 | 904.4 |
| 141 |  | 10.852 | 300 | 60 | 70.0 | 2.010 | 300 | 1189.8 |
| 142 |  | 10.852 | 300 | 60 | 70.0 | 2.010 | 400 | 1598.1 |
| 143 | Wang (2020) | 21.558 | 300 | 60 | 83.0 | 2.170 | 100 | 1089.3 |
| 144 |  | 21.558 | 300 | 60 | 83.0 | 2.170 | 200 | 1653.7 |
| 145 |  | 21.558 | 300 | 60 | 83.0 | 2.170 | 400 | 2588.8 |
| 146 |  | 21.558 | 300 | 60 | 83.0 | 2.170 | 800 | 5160.5 |
| 147 |  | 21.558 | 300 | 60 | 83.0 | 2.170 | 1200 | 6154.6 |
| 148 |  | 21.558 | 300 | 60 | 83.0 | 2.170 | 2000 | 9078.1 |
| 149 |  | 21.558 | 300 | 60 | 83.0 | 2.170 | 3200 | 13780.5 |
| 150 | Qin et al. (2010) | 11.030 | 300 | 60 | 69.0 | 2.180 | 100 | 505.9 |
| 151 |  | 11.030 | 300 | 60 | 69.0 | 2.180 | 200 | 732.3 |
| 152 |  | 11.030 | 300 | 60 | 69.0 | 2.180 | 400 | 1096.9 |
| 153 | Jiang et al. (2018) | 15.341 | 300 | 60 | 80.0 | 2.060 | 200 | 1389.5 |
| 154 |  | 15.341 | 300 | 60 | 80.0 | 2.060 | 400 | 2073.7 |
| 155 |  | 15.341 | 300 | 60 | 80.0 | 2.060 | 800 | 3379.0 |
| 156 | Yang (2022) | 11.017 | 300 | 60 | 72.5 | 2.210 | 400 | 2470.6 |
| 157 |  | 11.017 | 300 | 60 | 72.5 | 2.210 | 800 | 4034.9 |
| 158 |  | 11.017 | 300 | 60 | 72.5 | 2.210 | 1200 | 5672.0 |
| 159 |  | 11.017 | 300 | 60 | 72.5 | 2.210 | 1600 | 7005.9 |
| 160 |  | 12.732 | 300 | 60 | 78.5 | 2.175 | 400 | 2240.7 |
| 161 |  | 12.732 | 300 | 60 | 78.5 | 2.175 | 800 | 4182.6 |
| 162 |  | 12.732 | 300 | 60 | 78.5 | 2.175 | 1200 | 5663.9 |
| 163 |  | 12.732 | 300 | 60 | 78.5 | 2.175 | 1600 | 6933.6 |
| 164 |  | 9.533 | 300 | 60 | 66.5 | 2.230 | 400 | 2610.9 |
| 165 |  | 9.533 | 300 | 60 | 66.5 | 2.230 | 800 | 4292.9 |
| 166 |  | 9.533 | 300 | 60 | 66.5 | 2.230 | 1200 | 5861.9 |
| 167 |  | 9.533 | 300 | 60 | 66.5 | 2.230 | 1600 | 7192.5 |
| 168 |  | 29.206 | 300 | 60 | 100.0 | 1.930 | 400 | 1952.0 |
| 169 |  | 29.206 | 300 | 60 | 100.0 | 1.930 | 800 | 3149.7 |
| 170 |  | 29.206 | 300 | 60 | 100.0 | 1.930 | 1200 | 4390.1 |
| 171 |  | 29.206 | 300 | 60 | 100.0 | 1.930 | 1600 | 5327.3 |
| 172 |  | 1.394 | 300 | 60 | 0.0 | 1.900 | 400 | 1842.8 |
| 173 |  | 1.394 | 300 | 60 | 0.0 | 1.900 | 800 | 3141.9 |
| 174 |  | 1.394 | 300 | 60 | 0.0 | 1.900 | 1200 | 4360.7 |
| 175 |  | 1.394 | 300 | 60 | 0.0 | 1.900 | 1600 | 5512.5 |
| 176 | Lv et al. (2022) | 7.238 | 300 | 60 | 57.3 | 2.030 | 100 | 504.2 |
| 177 |  | 7.238 | 300 | 60 | 57.3 | 2.030 | 150 | 762.6 |
| 178 |  | 7.238 | 300 | 60 | 57.3 | 2.030 | 200 | 1008.4 |
| 179 |  | 7.238 | 300 | 60 | 57.3 | 2.030 | 300 | 1455.9 |
| 180 | Ma et al. (2021) | 9.452 | 300 | 80 | 66.6 | 2.050 | 300 | 757.5 |
| 181 |  | 9.452 | 300 | 80 | 66.6 | 2.050 | 600 | 1365.5 |
| 182 |  | 9.452 | 300 | 80 | 66.6 | 2.050 | 900 | 2103.0 |
| 183 |  | 9.452 | 300 | 80 | 66.6 | 2.050 | 1200 | 2730.9 |
| 184 | Wang (2021) | 20.271 | 300 | 60 | 80.0 | 2.240 | 100 | 1011.4 |
| 185 |  | 20.271 | 300 | 60 | 80.0 | 2.240 | 200 | 1389.3 |
| 186 |  | 20.271 | 300 | 60 | 80.0 | 2.240 | 400 | 2054.3 |
| 187 |  | 20.271 | 300 | 60 | 80.0 | 2.240 | 800 | 3253.6 |
| 188 |  | 20.271 | 300 | 60 | 80.0 | 2.240 | 2000 | 6217.6 |
| 189 |  | 20.271 | 300 | 60 | 80.0 | 2.240 | 3000 | 7878.0 |
| 190 |  | 24.959 | 300 | 60 | 87.5 | 2.240 | 100 | 1209.3 |
| 191 |  | 24.959 | 300 | 60 | 87.5 | 2.240 | 200 | 1605.4 |
| 192 |  | 24.959 | 300 | 60 | 87.5 | 2.240 | 400 | 2248.7 |
| 193 |  | 24.959 | 300 | 60 | 87.5 | 2.240 | 800 | 3630.8 |
| 194 |  | 24.959 | 300 | 60 | 87.5 | 2.240 | 2000 | 6901.3 |
| 195 |  | 24.959 | 300 | 60 | 87.5 | 2.240 | 3000 | 9304.2 |
| 196 |  | 31.943 | 300 | 60 | 95.0 | 2.240 | 100 | 1024.8 |
| 197 |  | 31.943 | 300 | 60 | 95.0 | 2.240 | 200 | 1656.8 |
| 198 |  | 31.943 | 300 | 60 | 95.0 | 2.240 | 400 | 2826.7 |
| 199 |  | 31.943 | 300 | 60 | 95.0 | 2.240 | 800 | 4349.8 |
| 200 |  | 31.943 | 300 | 60 | 95.0 | 2.240 | 2000 | 7473.6 |
| 201 |  | 31.943 | 300 | 60 | 95.0 | 2.240 | 3000 | 11115.5 |
| 202 |  | 14.786 | 300 | 60 | 64.0 | 2.310 | 100 | 1023.0 |
| 203 |  | 14.786 | 300 | 60 | 64.0 | 2.310 | 200 | 1269.5 |
| 204 |  | 14.786 | 300 | 60 | 64.0 | 2.310 | 400 | 2383.3 |
| 205 |  | 14.786 | 300 | 60 | 64.0 | 2.310 | 800 | 3802.8 |
| 206 |  | 14.786 | 300 | 60 | 64.0 | 2.310 | 2000 | 6984.7 |
| 207 |  | 14.786 | 300 | 60 | 64.0 | 2.310 | 3000 | 9343.3 |
| 208 |  | 17.956 | 300 | 60 | 75.5 | 2.310 | 100 | 1039.6 |
| 209 |  | 17.956 | 300 | 60 | 75.5 | 2.310 | 200 | 1776.7 |
| 210 |  | 17.956 | 300 | 60 | 75.5 | 2.310 | 400 | 2370.7 |
| 211 |  | 17.956 | 300 | 60 | 75.5 | 2.310 | 800 | 4361.9 |
| 212 |  | 17.956 | 300 | 60 | 75.5 | 2.310 | 2000 | 8406.2 |
| 213 |  | 17.956 | 300 | 60 | 75.5 | 2.310 | 3000 | 9836.4 |
| 214 |  | 21.992 | 300 | 60 | 87.0 | 2.310 | 100 | 1105.9 |
| 215 |  | 21.992 | 300 | 60 | 87.0 | 2.310 | 200 | 1780.0 |
| 216 |  | 21.992 | 300 | 60 | 87.0 | 2.310 | 400 | 2539.8 |
| 217 |  | 21.992 | 300 | 60 | 87.0 | 2.310 | 800 | 4501.0 |
| 218 |  | 21.992 | 300 | 60 | 87.0 | 2.310 | 2000 | 8588.4 |
| 219 |  | 21.992 | 300 | 60 | 87.0 | 2.310 | 3000 | 10734.2 |
| 220 | Tian et al. (2019) | 17.914 | 300 | 60 | 80.0 | 2.018 | 100 | 1009.8 |
| 221 |  | 17.914 | 300 | 60 | 80.0 | 2.018 | 200 | 1502.2 |
| 222 |  | 17.914 | 300 | 60 | 80.0 | 2.018 | 300 | 1943.5 |
| 223 |  | 14.570 | 300 | 60 | 75.8 | 2.018 | 100 | 882.2 |
| 224 |  | 14.570 | 300 | 60 | 75.8 | 2.018 | 200 | 1295.7 |
| 225 |  | 14.570 | 300 | 60 | 75.8 | 2.018 | 300 | 1729.3 |
| 226 |  | 14.193 | 300 | 60 | 75.6 | 2.018 | 100 | 849.3 |
| 227 |  | 14.193 | 300 | 60 | 75.6 | 2.018 | 200 | 1185.4 |
| 228 |  | 14.193 | 300 | 60 | 75.6 | 2.018 | 300 | 1509.3 |
| 229 |  | 12.167 | 300 | 60 | 73.1 | 2.018 | 100 | 683.0 |
| 230 |  | 12.167 | 300 | 60 | 73.1 | 2.018 | 200 | 1036.6 |
| 231 |  | 12.167 | 300 | 60 | 73.1 | 2.018 | 300 | 1308.1 |
| 232 | Wang (2012) | 0.489 | 300 | 40 | 13.5 | 1.941 | 100 | 357.9 |
| 233 |  | 0.489 | 300 | 40 | 13.5 | 1.941 | 200 | 574.4 |
| 234 |  | 0.489 | 300 | 40 | 13.5 | 1.941 | 300 | 793.5 |
| 235 |  | 0.489 | 300 | 40 | 13.5 | 1.941 | 400 | 1064.8 |
| 236 |  | 1.042 | 300 | 40 | 31.1 | 2.061 | 100 | 403.4 |
| 237 |  | 1.042 | 300 | 40 | 31.1 | 2.061 | 200 | 653.4 |
| 238 |  | 1.042 | 300 | 40 | 31.1 | 2.061 | 300 | 982.8 |
| 239 |  | 1.042 | 300 | 40 | 31.1 | 2.061 | 400 | 1232.7 |
| 240 |  | 2.195 | 300 | 40 | 48.3 | 2.095 | 100 | 548.0 |
| 241 |  | 2.195 | 300 | 40 | 48.3 | 2.095 | 200 | 869.5 |
| 242 |  | 2.195 | 300 | 40 | 48.3 | 2.095 | 300 | 1194.4 |
| 243 |  | 2.195 | 300 | 40 | 48.3 | 2.095 | 400 | 1459.3 |
| 244 |  | 4.551 | 300 | 40 | 65.7 | 2.098 | 100 | 624.5 |
| 245 |  | 4.551 | 300 | 40 | 65.7 | 2.098 | 200 | 956.3 |
| 246 |  | 4.551 | 300 | 40 | 65.7 | 2.098 | 300 | 1401.8 |
| 247 |  | 4.551 | 300 | 40 | 65.7 | 2.098 | 400 | 1681.2 |
| 248 |  | 9.603 | 300 | 40 | 83.1 | 1.996 | 100 | 660.4 |
| 249 |  | 9.603 | 300 | 40 | 83.1 | 1.996 | 200 | 1075.5 |
| 250 |  | 9.603 | 300 | 40 | 83.1 | 1.996 | 300 | 1494.4 |
| 251 |  | 9.603 | 300 | 40 | 83.1 | 1.996 | 400 | 1773.7 |
| 252 | Jiang et al. (2014) | 22.596 | 300 | 60 | 90.6 | 2.050 | 400 | 1702.4 |
| 253 |  | 22.596 | 300 | 60 | 90.6 | 2.050 | 800 | 3224.6 |
| 254 |  | 22.596 | 300 | 60 | 90.6 | 2.050 | 1600 | 5311.2 |
| 255 |  | 22.596 | 300 | 60 | 90.6 | 2.100 | 400 | 1892.9 |
| 256 |  | 22.596 | 300 | 60 | 90.6 | 2.100 | 800 | 3225.1 |
| 257 |  | 22.596 | 300 | 60 | 90.6 | 2.100 | 1600 | 5376.5 |
| 258 |  | 22.596 | 300 | 60 | 90.6 | 2.170 | 400 | 2107.1 |
| 259 |  | 22.596 | 300 | 60 | 90.6 | 2.170 | 800 | 3479.9 |
| 260 |  | 22.596 | 300 | 60 | 90.6 | 2.170 | 1600 | 5509.2 |
| 261 |  | 22.596 | 300 | 60 | 90.6 | 2.270 | 400 | 2440.5 |
| 262 |  | 22.596 | 300 | 60 | 90.6 | 2.270 | 800 | 3654.6 |
| 263 |  | 22.596 | 300 | 60 | 90.6 | 2.270 | 1600 | 5756.9 |
| 264 | Chu et al. (2011) | 11.512 | 300 | 60 | 72.0 | 2.250 | 200 | 1169.5 |
| 265 |  | 11.512 | 300 | 60 | 72.0 | 2.250 | 500 | 2510.4 |
| 266 |  | 11.512 | 300 | 60 | 72.0 | 2.250 | 1200 | 5118.5 |
| 267 |  | 11.512 | 300 | 60 | 72.0 | 2.250 | 2000 | 8165.6 |
| 268 |  | 11.512 | 300 | 60 | 72.0 | 2.250 | 2500 | 9824.4 |
| 269 |  | 11.512 | 300 | 60 | 72.0 | 2.170 | 200 | 896.6 |
| 270 |  | 11.512 | 300 | 60 | 72.0 | 2.170 | 500 | 2275.9 |
| 271 |  | 11.512 | 300 | 60 | 72.0 | 2.170 | 1200 | 4827.6 |
| 272 |  | 11.512 | 300 | 60 | 72.0 | 2.170 | 2000 | 7655.2 |
| 273 |  | 11.512 | 300 | 60 | 72.0 | 2.170 | 2500 | 9172.4 |
| 274 | Shi et al. (2014) | 1.132 | 300 | 60 | 32.0 | 2.119 | 200 | 651.3 |
| 275 |  | 1.132 | 300 | 60 | 32.0 | 2.119 | 400 | 1105.3 |
| 276 |  | 1.132 | 300 | 60 | 32.0 | 2.119 | 800 | 2398.0 |
| 277 | Chen (2010) | 18.476 | 300 | 60 | 81.0 | 1.880 | 100 | 805.6 |
| 278 |  | 18.476 | 300 | 60 | 81.0 | 1.880 | 200 | 1101.6 |
| 279 |  | 18.476 | 300 | 60 | 81.0 | 1.880 | 400 | 1462.0 |
| 280 |  | 18.476 | 300 | 60 | 81.0 | 1.880 | 800 | 2081.8 |
| 281 | Wang et al. (2023) | 15.172 | 300 | 60 | 78.0 | 2.110 | 200 | 983.9 |
| 282 |  | 15.172 | 300 | 60 | 78.0 | 2.110 | 400 | 1790.3 |
| 283 |  | 15.172 | 300 | 60 | 78.0 | 2.110 | 600 | 2443.6 |
| 284 |  | 15.172 | 300 | 60 | 78.0 | 2.110 | 800 | 3064.5 |
| 285 | Chu (2014) | 22.248 | 300 | 60 | 88.0 | 2.254 | 200 | 1219.0 |
| 286 |  | 22.248 | 300 | 60 | 88.0 | 2.254 | 500 | 2521.0 |
| 287 |  | 22.248 | 300 | 60 | 88.0 | 2.254 | 1200 | 5156.0 |
| 288 |  | 22.248 | 300 | 60 | 88.0 | 2.254 | 2000 | 8187.0 |
| 289 |  | 22.248 | 300 | 60 | 88.0 | 2.254 | 2500 | 9830.0 |
| 290 |  | 22.248 | 300 | 60 | 88.0 | 2.218 | 200 | 1219.0 |
| 291 |  | 22.248 | 300 | 60 | 88.0 | 2.218 | 500 | 2512.0 |
| 292 |  | 22.248 | 300 | 60 | 88.0 | 2.218 | 1200 | 5102.0 |
| 293 |  | 22.248 | 300 | 60 | 88.0 | 2.218 | 2000 | 8173.0 |
| 294 |  | 22.248 | 300 | 60 | 88.0 | 2.218 | 2500 | 9778.0 |
| 295 | Zhao et al. (2008) | 0.984 | 300 | 60 | 45.0 | 2.075 | 200 | 743.4 |
| 296 |  | 0.984 | 300 | 60 | 45.0 | 2.075 | 600 | 1828.1 |
| 297 |  | 0.984 | 300 | 60 | 45.0 | 2.075 | 1000 | 2538.5 |
| 298 |  | 0.984 | 300 | 60 | 45.0 | 2.075 | 2000 | 4242.7 |
| 299 |  | 0.984 | 300 | 60 | 45.0 | 2.075 | 3000 | 7301.5 |
| 300 |  | 0.984 | 300 | 60 | 45.0 | 2.075 | 4000 | 8050.3 |
| 301 |  | 0.984 | 300 | 60 | 45.0 | 2.075 | 5000 | 11081.6 |
| 302 | Han (2010) | 3.105 | 300 | 20 | 32.5 | 1.940 | 200 | 763.7 |
| 303 |  | 3.105 | 300 | 20 | 32.5 | 1.940 | 400 | 1440.0 |
| 304 |  | 3.105 | 300 | 20 | 32.5 | 1.940 | 600 | 2096.1 |
| 305 |  | 3.105 | 300 | 20 | 32.5 | 1.940 | 1000 | 3344.3 |
| 306 |  | 22.146 | 300 | 60 | 87.8 | 2.010 | 200 | 1148.3 |
| 307 |  | 22.146 | 300 | 60 | 87.8 | 2.010 | 400 | 1791.3 |
| 308 |  | 22.146 | 300 | 60 | 87.8 | 2.010 | 600 | 2289.0 |
| 309 |  | 22.146 | 300 | 60 | 87.8 | 2.010 | 1000 | 3730.5 |
| 310 | Lian (2010) | 3.105 | 300 | 20 | 32.5 | 2.060 | 200 | 763.1 |
| 311 |  | 3.105 | 300 | 20 | 32.5 | 2.060 | 600 | 2103.4 |
| 312 |  | 3.105 | 300 | 20 | 32.5 | 2.060 | 1000 | 3349.2 |
| 313 |  | 3.105 | 300 | 20 | 32.5 | 2.060 | 2000 | 6566.3 |
| 314 |  | 3.105 | 500 | 20 | 32.5 | 2.060 | 200 | 851.2 |
| 315 |  | 3.105 | 500 | 20 | 32.5 | 2.060 | 600 | 2392.0 |
| 316 |  | 3.105 | 500 | 20 | 32.5 | 2.060 | 1000 | 3639.4 |
| 317 |  | 3.105 | 500 | 20 | 32.5 | 2.060 | 2000 | 6060.8 |
| 318 |  | 8.573 | 500 | 60 | 57.0 | 2.052 | 200 | 1203.8 |
| 319 |  | 8.573 | 500 | 60 | 57.0 | 2.052 | 600 | 2273.9 |
| 320 |  | 8.573 | 500 | 60 | 57.0 | 2.052 | 1000 | 3418.3 |
| 321 |  | 8.573 | 500 | 60 | 57.0 | 2.052 | 2000 | 6108.3 |
| 322 |  | 11.008 | 300 | 60 | 68.5 | 2.070 | 200 | 818.5 |
| 323 |  | 11.008 | 300 | 60 | 68.5 | 2.070 | 600 | 2316.6 |
| 324 |  | 11.008 | 300 | 60 | 68.5 | 2.070 | 1000 | 3830.1 |
| 325 |  | 11.008 | 300 | 60 | 68.5 | 2.070 | 2000 | 7243.2 |
| 326 |  | 11.008 | 500 | 60 | 68.5 | 2.070 | 200 | 1031.3 |
| 327 |  | 11.008 | 500 | 60 | 68.5 | 2.070 | 600 | 2208.5 |
| 328 |  | 11.008 | 500 | 60 | 68.5 | 2.070 | 1000 | 3691.1 |
| 329 |  | 11.008 | 500 | 60 | 68.5 | 2.070 | 2000 | 6625.5 |
| 330 |  | 19.956 | 300 | 60 | 83.0 | 2.107 | 200 | 955.7 |
| 331 |  | 19.956 | 300 | 60 | 83.0 | 2.107 | 400 | 1640.2 |
| 332 |  | 19.956 | 300 | 60 | 83.0 | 2.107 | 800 | 3035.1 |
| 333 |  | 19.956 | 300 | 60 | 83.0 | 2.107 | 1200 | 4481.6 |
| 334 |  | 19.956 | 500 | 60 | 83.0 | 2.107 | 200 | 942.8 |
| 335 |  | 19.956 | 500 | 60 | 83.0 | 2.107 | 400 | 1717.7 |
| 336 |  | 19.956 | 500 | 60 | 83.0 | 2.107 | 1000 | 3345.0 |
| 337 |  | 19.956 | 500 | 60 | 83.0 | 2.107 | 2000 | 6199.3 |
| 338 |  | 24.396 | 500 | 100 | 83.0 | 2.107 | 200 | 988.2 |
| 339 |  | 24.396 | 500 | 100 | 83.0 | 2.107 | 600 | 2305.9 |
| 340 |  | 24.396 | 500 | 100 | 83.0 | 2.107 | 1000 | 3576.5 |
| 341 |  | 24.396 | 500 | 100 | 83.0 | 2.107 | 2000 | 6776.5 |
| 342 |  | 19.956 | 300 | 60 | 83.0 | 2.170 | 200 | 958.1 |
| 343 |  | 19.956 | 300 | 60 | 83.0 | 2.170 | 400 | 1656.7 |
| 344 |  | 19.956 | 300 | 60 | 83.0 | 2.170 | 800 | 3043.9 |
| 345 |  | 19.956 | 300 | 60 | 83.0 | 2.170 | 1200 | 4481.0 |
| 346 |  | 19.956 | 500 | 60 | 83.0 | 2.170 | 200 | 808.4 |
| 347 |  | 19.956 | 500 | 60 | 83.0 | 2.170 | 400 | 1556.9 |
| 348 |  | 19.956 | 500 | 60 | 83.0 | 2.170 | 800 | 3153.7 |
| 349 |  | 19.956 | 500 | 60 | 83.0 | 2.170 | 1200 | 4431.1 |
| 350 |  | 24.396 | 500 | 100 | 83.0 | 2.170 | 200 | 1115.3 |
| 351 |  | 24.396 | 500 | 100 | 83.0 | 2.170 | 400 | 1758.0 |
| 352 |  | 24.396 | 500 | 100 | 83.0 | 2.170 | 800 | 3156.9 |
| 353 |  | 24.396 | 500 | 100 | 83.0 | 2.170 | 1200 | 4593.6 |
| 354 |  | 27.322 | 300 | 60 | 94.0 | 2.134 | 200 | 996.2 |
| 355 |  | 27.322 | 300 | 60 | 94.0 | 2.134 | 600 | 2222.2 |
| 356 |  | 27.322 | 300 | 60 | 94.0 | 2.134 | 1000 | 3708.8 |
| 357 |  | 27.322 | 300 | 60 | 94.0 | 2.134 | 2000 | 7080.5 |
| 358 |  | 27.322 | 500 | 60 | 94.0 | 2.134 | 200 | 950.2 |
| 359 |  | 27.322 | 500 | 60 | 94.0 | 2.134 | 600 | 2283.5 |
| 360 |  | 27.322 | 500 | 60 | 94.0 | 2.134 | 1000 | 3693.5 |
| 361 |  | 27.322 | 500 | 60 | 94.0 | 2.134 | 2000 | 7111.1 |
| 362 |  | 37.486 | 500 | 100 | 94.0 | 2.134 | 200 | 955.0 |
| 363 |  | 37.486 | 500 | 100 | 94.0 | 2.134 | 600 | 2181.5 |
| 364 |  | 37.486 | 500 | 100 | 94.0 | 2.134 | 1000 | 3781.2 |
| 365 |  | 37.486 | 500 | 100 | 94.0 | 2.134 | 2000 | 7248.5 |
| 366 |  | 27.322 | 300 | 60 | 94.0 | 2.078 | 200 | 985.1 |
| 367 |  | 27.322 | 300 | 60 | 94.0 | 2.078 | 600 | 2223.9 |
| 368 |  | 27.322 | 300 | 60 | 94.0 | 2.078 | 1000 | 3701.5 |
| 369 |  | 27.322 | 300 | 60 | 94.0 | 2.078 | 2000 | 7089.6 |
| 370 |  | 27.322 | 500 | 60 | 94.0 | 2.078 | 200 | 970.1 |
| 371 |  | 27.322 | 500 | 60 | 94.0 | 2.078 | 600 | 2044.8 |
| 372 |  | 27.322 | 500 | 60 | 94.0 | 2.078 | 1000 | 3656.7 |
| 373 |  | 27.322 | 500 | 60 | 94.0 | 2.078 | 2000 | 6611.9 |
| 374 |  | 37.486 | 500 | 100 | 94.0 | 2.078 | 200 | 892.5 |
| 375 |  | 37.486 | 500 | 100 | 94.0 | 2.078 | 600 | 2128.7 |
| 376 |  | 37.486 | 500 | 100 | 94.0 | 2.078 | 1000 | 3658.9 |
| 377 |  | 37.486 | 500 | 100 | 94.0 | 2.078 | 2000 | 6824.3 |
| 378 |  | 1.529 | 101 | 20 | 14.0 | 2.033 | 100 | 551.6 |
| 379 |  | 1.529 | 101 | 20 | 14.0 | 2.033 | 200 | 1056.2 |
| 380 |  | 1.529 | 101 | 20 | 14.0 | 2.033 | 400 | 1602.3 |
| 381 |  | 1.529 | 101 | 20 | 14.0 | 2.033 | 600 | 2278.1 |
| 382 |  | 1.529 | 300 | 20 | 14.0 | 2.033 | 200 | 973.4 |
| 383 |  | 1.529 | 300 | 20 | 14.0 | 2.033 | 600 | 2112.4 |
| 384 |  | 1.529 | 300 | 20 | 14.0 | 2.033 | 1000 | 3458.6 |
| 385 |  | 1.529 | 300 | 20 | 14.0 | 2.033 | 2000 | 6047.3 |
| 386 |  | 1.529 | 500 | 20 | 14.0 | 2.033 | 200 | 724.9 |
| 387 |  | 1.529 | 500 | 20 | 14.0 | 2.033 | 600 | 2029.6 |
| 388 |  | 1.529 | 500 | 20 | 14.0 | 2.033 | 1000 | 3313.6 |
| 389 |  | 1.529 | 500 | 20 | 14.0 | 2.033 | 2000 | 5778.1 |
| 390 |  | 6.502 | 500 | 40 | 56.0 | 2.119 | 200 | 943.0 |
| 391 |  | 6.502 | 500 | 40 | 56.0 | 2.119 | 400 | 1762.7 |
| 392 |  | 6.502 | 500 | 40 | 56.0 | 2.119 | 800 | 3251.9 |
| 393 |  | 6.502 | 500 | 40 | 56.0 | 2.119 | 1200 | 4414.3 |
| 394 |  | 6.502 | 500 | 40 | 56.0 | 2.119 | 1600 | 5706.0 |
| 395 |  | 6.502 | 500 | 40 | 56.0 | 2.119 | 2000 | 6839.9 |
| 396 |  | 9.670 | 500 | 60 | 64.5 | 2.148 | 200 | 1258.2 |
| 397 |  | 9.670 | 500 | 60 | 64.5 | 2.148 | 400 | 2124.3 |
| 398 |  | 9.670 | 500 | 60 | 64.5 | 2.148 | 800 | 3291.7 |
| 399 |  | 9.670 | 500 | 60 | 64.5 | 2.148 | 1200 | 4474.6 |
| 400 |  | 9.670 | 500 | 60 | 64.5 | 2.148 | 1600 | 5784.8 |
| 401 |  | 9.670 | 500 | 60 | 64.5 | 2.148 | 2000 | 6885.1 |
| 402 |  | 12.733 | 500 | 80 | 70.4 | 2.188 | 200 | 1191.8 |
| 403 |  | 12.733 | 500 | 80 | 70.4 | 2.188 | 400 | 1823.0 |
| 404 |  | 12.733 | 500 | 80 | 70.4 | 2.188 | 800 | 3299.7 |
| 405 |  | 12.733 | 500 | 80 | 70.4 | 2.188 | 1200 | 4821.1 |
| 406 |  | 12.733 | 500 | 80 | 70.4 | 2.188 | 1600 | 6124.1 |
| 407 |  | 12.733 | 500 | 80 | 70.4 | 2.188 | 2000 | 7005.7 |
| 408 |  | 15.997 | 500 | 100 | 73.7 | 2.217 | 200 | 1044.8 |
| 409 |  | 15.997 | 500 | 100 | 73.7 | 2.217 | 400 | 2049.0 |
| 410 |  | 15.997 | 500 | 100 | 73.7 | 2.217 | 800 | 3368.3 |
| 411 |  | 15.997 | 500 | 100 | 73.7 | 2.217 | 1200 | 4715.6 |
| 412 |  | 15.997 | 500 | 100 | 73.7 | 2.217 | 1600 | 6295.6 |
| 413 |  | 15.997 | 500 | 100 | 73.7 | 2.217 | 2000 | 7457.6 |
| 414 | Asghari et al. (2003) | 3.153 | 101 | 13 | 45.0 | 1.800 | 25 | 151.7 |
| 415 |  | 3.153 | 101 | 13 | 45.0 | 1.800 | 55 | 216.3 |
| 416 |  | 3.153 | 101 | 13 | 45.0 | 1.800 | 110 | 442.7 |
| 417 |  | 3.153 | 101 | 13 | 45.0 | 1.800 | 300 | 764.4 |
| 418 |  | 3.153 | 101 | 13 | 45.0 | 1.800 | 500 | 1397.5 |
| 419 |  | 3.153 | 101 | 13 | 45.0 | 1.800 | 1000 | 2804.1 |
| 420 | Tao et al. (2022) | 6.676 | 101 | 20 | 30.0 | 1.740 | 100 | 277.2 |
| 421 |  | 6.676 | 101 | 20 | 30.0 | 1.740 | 200 | 368.6 |
| 422 |  | 8.094 | 101 | 20 | 50.0 | 1.740 | 100 | 327.6 |
| 423 |  | 8.094 | 101 | 20 | 50.0 | 1.740 | 200 | 462.1 |
| 424 |  | 9.815 | 101 | 20 | 70.0 | 1.740 | 100 | 356.7 |
| 425 |  | 9.815 | 101 | 20 | 70.0 | 1.740 | 200 | 617.5 |
| 426 | Xu et al. (2021) | 1.504 | 101 | 8 | 22.0 | 1.730 | 300 | 1195.9 |
| 427 |  | 1.504 | 101 | 8 | 22.0 | 1.730 | 600 | 2142.3 |
| 428 |  | 1.504 | 101 | 8 | 22.0 | 1.730 | 900 | 3093.3 |
| 429 |  | 2.728 | 292 | 60 | 35.0 | 1.730 | 300 | 1208.7 |
| 430 |  | 2.728 | 292 | 60 | 35.0 | 1.730 | 600 | 2360.2 |
| 431 |  | 2.728 | 292 | 60 | 35.0 | 1.730 | 900 | 3517.1 |
| 432 |  | 2.728 | 292 | 60 | 35.0 | 1.730 | 1200 | 4600.3 |
| 433 |  | 5.543 | 292 | 60 | 55.0 | 1.730 | 300 | 1408.2 |
| 434 |  | 5.543 | 292 | 60 | 55.0 | 1.730 | 600 | 2537.1 |
| 435 |  | 5.543 | 292 | 60 | 55.0 | 1.730 | 900 | 3765.8 |
| 436 |  | 5.543 | 292 | 60 | 55.0 | 1.730 | 1200 | 5086.7 |
| 437 |  | 14.181 | 292 | 60 | 79.0 | 1.730 | 300 | 1646.2 |
| 438 |  | 14.181 | 292 | 60 | 79.0 | 1.730 | 600 | 2775.5 |
| 439 |  | 14.181 | 292 | 60 | 79.0 | 1.730 | 900 | 4204.7 |
| 440 |  | 14.181 | 292 | 60 | 79.0 | 1.730 | 1200 | 5290.9 |
| 441 |  | 5.543 | 150 | 60 | 55.0 | 1.730 | 100 | 771.4 |
| 442 |  | 5.543 | 150 | 60 | 55.0 | 1.730 | 300 | 1607.1 |
| 443 |  | 5.543 | 150 | 60 | 55.0 | 1.730 | 600 | 3018.1 |
| 444 |  | 5.543 | 150 | 60 | 55.0 | 1.730 | 900 | 4149.5 |
| 445 |  | 4.375 | 150 | 30 | 55.0 | 1.730 | 100 | 528.3 |
| 446 |  | 4.375 | 150 | 30 | 55.0 | 1.730 | 300 | 1407.9 |
| 447 |  | 4.375 | 150 | 30 | 55.0 | 1.730 | 600 | 2628.1 |
| 448 |  | 4.375 | 150 | 30 | 55.0 | 1.730 | 900 | 3477.1 |
| 449 |  | 4.084 | 150 | 30 | 55.0 | 1.730 | 100 | 549.1 |
| 450 |  | 4.084 | 150 | 30 | 55.0 | 1.730 | 300 | 1386.4 |
| 451 |  | 4.084 | 150 | 30 | 55.0 | 1.730 | 600 | 2452.9 |
| 452 |  | 4.084 | 150 | 30 | 55.0 | 1.730 | 900 | 3444.1 |
| 453 |  | 5.543 | 101 | 60 | 55.0 | 1.730 | 100 | 736.7 |
| 454 |  | 5.543 | 101 | 60 | 55.0 | 1.730 | 300 | 1688.9 |
| 455 |  | 5.543 | 101 | 60 | 55.0 | 1.730 | 600 | 3457.5 |
| 456 |  | 5.543 | 101 | 60 | 55.0 | 1.730 | 900 | 4702.0 |
| 457 |  | 3.988 | 101 | 20 | 55.0 | 1.730 | 100 | 659.8 |
| 458 |  | 3.988 | 101 | 20 | 55.0 | 1.730 | 300 | 1514.8 |
| 459 |  | 3.988 | 101 | 20 | 55.0 | 1.730 | 600 | 2681.3 |
| 460 |  | 3.988 | 101 | 20 | 55.0 | 1.730 | 900 | 3595.7 |
| 461 |  | 3.704 | 101 | 20 | 55.0 | 1.730 | 100 | 552.7 |
| 462 |  | 3.704 | 101 | 20 | 55.0 | 1.730 | 300 | 1429.9 |
| 463 |  | 3.704 | 101 | 20 | 55.0 | 1.730 | 600 | 2489.1 |
| 464 |  | 3.704 | 101 | 20 | 55.0 | 1.730 | 900 | 3460.6 |
| 465 | Zhang et al. (2016) | 0.953 | 101 | 5 | 0.0 | 1.567 | 100 | 436.3 |
| 466 |  | 0.953 | 101 | 5 | 0.0 | 1.567 | 300 | 1204.7 |
| 467 |  | 0.953 | 101 | 5 | 0.0 | 1.567 | 600 | 2148.4 |
| 468 |  | 0.953 | 101 | 5 | 0.0 | 1.567 | 900 | 3151.1 |
| 469 |  | 5.415 | 101 | 60 | 50.0 | 1.567 | 100 | 738.7 |
| 470 |  | 5.415 | 101 | 60 | 50.0 | 1.567 | 300 | 1712.6 |
| 471 |  | 5.415 | 101 | 60 | 50.0 | 1.567 | 600 | 3425.1 |
| 472 |  | 5.415 | 101 | 60 | 50.0 | 1.567 | 900 | 4686.7 |
| 473 |  | 3.809 | 101 | 20 | 50.0 | 1.567 | 100 | 666.7 |
| 474 |  | 3.809 | 101 | 20 | 50.0 | 1.567 | 300 | 1508.1 |
| 475 |  | 3.809 | 101 | 20 | 50.0 | 1.567 | 600 | 2485.1 |
| 476 |  | 3.809 | 101 | 20 | 50.0 | 1.567 | 900 | 3438.8 |
| 477 |  | 3.546 | 101 | 20 | 50.0 | 1.567 | 100 | 563.3 |
| 478 |  | 3.546 | 101 | 20 | 50.0 | 1.567 | 300 | 1430.2 |
| 479 |  | 3.546 | 101 | 20 | 50.0 | 1.567 | 600 | 2690.8 |
| 480 |  | 3.546 | 101 | 20 | 50.0 | 1.567 | 900 | 3628.0 |
| 481 | Zhao et al. (2018) | 0.114 | 101 | 1 | 0.0 | 1.873 | 200 | 436.1 |
| 482 |  | 0.114 | 101 | 1 | 0.0 | 1.873 | 400 | 711.3 |
| 483 |  | 0.114 | 101 | 1 | 0.0 | 1.873 | 800 | 1140.1 |
| 484 |  | 0.320 | 101 | 20 | 20.0 | 1.873 | 200 | 401.6 |
| 485 |  | 0.320 | 101 | 20 | 20.0 | 1.873 | 400 | 730.6 |
| 486 |  | 0.320 | 101 | 20 | 20.0 | 1.873 | 800 | 1260.3 |
| 487 |  | 0.536 | 101 | 20 | 30.0 | 1.873 | 200 | 382.7 |
| 488 |  | 0.536 | 101 | 20 | 30.0 | 1.873 | 400 | 689.5 |
| 489 |  | 0.536 | 101 | 20 | 30.0 | 1.873 | 800 | 1296.0 |
| 490 |  | 1.508 | 101 | 20 | 50.0 | 1.873 | 200 | 450.2 |
| 491 |  | 1.508 | 101 | 20 | 50.0 | 1.873 | 400 | 851.6 |
| 492 |  | 1.508 | 101 | 20 | 50.0 | 1.873 | 800 | 1705.7 |
| 493 |  | 4.241 | 101 | 20 | 70.0 | 1.873 | 200 | 680.8 |
| 494 |  | 4.241 | 101 | 20 | 70.0 | 1.873 | 400 | 1173.4 |
| 495 |  | 4.241 | 101 | 20 | 70.0 | 1.873 | 800 | 2159.9 |
| 496 |  | 1.349 | 101 | 16 | 50.0 | 1.873 | 200 | 469.6 |
| 497 |  | 1.349 | 101 | 16 | 50.0 | 1.873 | 400 | 821.5 |
| 498 |  | 1.349 | 101 | 16 | 50.0 | 1.873 | 800 | 1544.4 |
| 499 |  | 1.066 | 101 | 10 | 50.0 | 1.873 | 200 | 406.9 |
| 500 |  | 1.066 | 101 | 10 | 50.0 | 1.873 | 400 | 819.7 |
| 501 |  | 1.066 | 101 | 10 | 50.0 | 1.873 | 800 | 1516.0 |
| 502 |  | 1.295 | 101 | 20 | 50.0 | 1.873 | 200 | 383.6 |
| 503 |  | 1.295 | 101 | 20 | 50.0 | 1.873 | 400 | 817.9 |
| 504 |  | 1.295 | 101 | 20 | 50.0 | 1.873 | 800 | 1533.7 |
| 505 | Zhao et al. (2019) | 0.160 | 101 | 2 | 0.0 | 1.885 | 200 | 307.8 |
| 506 |  | 0.160 | 101 | 2 | 0.0 | 1.885 | 400 | 474.2 |
| 507 |  | 0.160 | 101 | 2 | 0.0 | 1.885 | 800 | 830.2 |
| 508 |  | 0.252 | 101 | 15 | 10.0 | 1.885 | 200 | 374.0 |
| 509 |  | 0.252 | 101 | 15 | 10.0 | 1.885 | 400 | 562.0 |
| 510 |  | 0.252 | 101 | 15 | 10.0 | 1.885 | 800 | 1030.0 |
| 511 |  | 0.625 | 101 | 15 | 30.0 | 1.885 | 200 | 410.9 |
| 512 |  | 0.625 | 101 | 15 | 30.0 | 1.885 | 400 | 615.1 |
| 513 |  | 0.625 | 101 | 15 | 30.0 | 1.885 | 800 | 1147.5 |
| 514 |  | 1.559 | 101 | 15 | 50.0 | 1.885 | 200 | 400.8 |
| 515 |  | 1.559 | 101 | 15 | 50.0 | 1.885 | 400 | 699.8 |
| 516 |  | 1.559 | 101 | 15 | 50.0 | 1.885 | 800 | 1409.2 |
| 517 |  | 3.838 | 101 | 15 | 70.0 | 1.885 | 200 | 521.9 |
| 518 |  | 3.838 | 101 | 15 | 70.0 | 1.885 | 400 | 965.7 |
| 519 |  | 3.838 | 101 | 15 | 70.0 | 1.885 | 800 | 1785.8 |
| 520 | Chen et al. (2023) | 2.187 | 101 | 20 | 20.0 | 1.650 | 100 | 259.9 |
| 521 |  | 2.187 | 101 | 20 | 20.0 | 1.650 | 250 | 542.8 |
| 522 |  | 2.187 | 101 | 20 | 20.0 | 1.650 | 400 | 899.8 |
| 523 |  | 2.187 | 101 | 20 | 20.0 | 1.650 | 550 | 1140.1 |
| 524 |  | 2.187 | 101 | 20 | 20.0 | 1.650 | 700 | 1331.8 |
| 525 |  | 2.983 | 101 | 20 | 30.0 | 1.750 | 100 | 269.3 |
| 526 |  | 2.983 | 101 | 20 | 30.0 | 1.750 | 250 | 590.3 |
| 527 |  | 2.983 | 101 | 20 | 30.0 | 1.750 | 400 | 948.3 |
| 528 |  | 2.983 | 101 | 20 | 30.0 | 1.750 | 550 | 1191.7 |
| 529 |  | 2.983 | 101 | 20 | 30.0 | 1.750 | 700 | 1451.5 |
| 530 |  | 3.824 | 101 | 20 | 40.0 | 1.850 | 100 | 279.1 |
| 531 |  | 3.824 | 101 | 20 | 40.0 | 1.850 | 250 | 636.3 |
| 532 |  | 3.824 | 101 | 20 | 40.0 | 1.850 | 400 | 967.4 |
| 533 |  | 3.824 | 101 | 20 | 40.0 | 1.850 | 550 | 1254.0 |
| 534 |  | 3.824 | 101 | 20 | 40.0 | 1.850 | 700 | 1531.0 |
| 535 |  | 4.955 | 101 | 20 | 50.0 | 1.950 | 100 | 294.0 |
| 536 |  | 4.955 | 101 | 20 | 50.0 | 1.950 | 250 | 721.4 |
| 537 |  | 4.955 | 101 | 20 | 50.0 | 1.950 | 400 | 1096.7 |
| 538 |  | 4.955 | 101 | 20 | 50.0 | 1.950 | 550 | 1372.1 |
| 539 |  | 4.955 | 101 | 20 | 50.0 | 1.950 | 700 | 1762.3 |
| 540 | Tan et al. (2015) | 14.406 | 101 | 40 | 74.0 | 1.830 | 100 | 442.4 |
| 541 |  | 14.406 | 101 | 40 | 74.0 | 1.830 | 200 | 748.2 |
| 542 |  | 14.406 | 101 | 40 | 74.0 | 1.830 | 300 | 971.8 |
| 543 |  | 14.406 | 101 | 40 | 74.0 | 1.830 | 400 | 1326.7 |
| 544 |  | 7.206 | 101 | 20 | 60.0 | 1.760 | 100 | 362.2 |
| 545 |  | 7.206 | 101 | 20 | 60.0 | 1.760 | 200 | 659.0 |
| 546 |  | 7.206 | 101 | 20 | 60.0 | 1.760 | 300 | 927.1 |
| 547 |  | 7.206 | 101 | 20 | 60.0 | 1.760 | 400 | 1194.0 |
| 548 |  | 3.655 | 101 | 10 | 37.0 | 1.750 | 100 | 337.1 |
| 549 |  | 3.655 | 101 | 10 | 37.0 | 1.750 | 200 | 652.2 |
| 550 |  | 3.655 | 101 | 10 | 37.0 | 1.750 | 300 | 915.3 |
| 551 |  | 3.655 | 101 | 10 | 37.0 | 1.750 | 400 | 1187.5 |
| 552 |  | 1.852 | 101 | 5 | 100.0 | 1.700 | 100 | 335.9 |
| 553 |  | 1.852 | 101 | 5 | 100.0 | 1.700 | 200 | 650.1 |
| 554 |  | 1.852 | 101 | 5 | 100.0 | 1.700 | 300 | 903.5 |
| 555 |  | 1.852 | 101 | 5 | 100.0 | 1.700 | 400 | 1187.2 |
| 556 |  | 0.711 | 101 | 2 | 100.0 | 1.630 | 100 | 337.1 |
| 557 |  | 0.711 | 101 | 2 | 100.0 | 1.630 | 200 | 646.1 |
| 558 |  | 0.711 | 101 | 2 | 100.0 | 1.630 | 300 | 891.8 |
| 559 |  | 0.711 | 101 | 2 | 100.0 | 1.630 | 400 | 1180.7 |
| 560 | Wan et al. (2024) | 4.092 | 101 | 20 | 58.0 | 2.060 | 200 | 925.2 |
| 561 |  | 4.092 | 101 | 20 | 58.0 | 2.060 | 700 | 2817.0 |
| 562 | Wang et al. (2023) | 0.018 | 101 | 2 | 0.0 | 1.610 | 100 | 190.1 |
| 563 |  | 0.018 | 101 | 2 | 0.0 | 1.610 | 200 | 289.4 |
| 564 |  | 0.018 | 101 | 2 | 0.0 | 1.610 | 300 | 392.9 |
| 565 |  | 0.018 | 101 | 2 | 0.0 | 1.610 | 400 | 498.5 |
| 566 |  | 0.094 | 101 | 20 | 16.0 | 1.860 | 100 | 277.2 |
| 567 |  | 0.094 | 101 | 20 | 16.0 | 1.860 | 200 | 417.1 |
| 568 |  | 0.094 | 101 | 20 | 16.0 | 1.860 | 300 | 550.4 |
| 569 |  | 0.094 | 101 | 20 | 16.0 | 1.860 | 400 | 743.8 |
| 570 |  | 0.312 | 101 | 20 | 32.0 | 1.980 | 100 | 244.1 |
| 571 |  | 0.312 | 101 | 20 | 32.0 | 1.980 | 200 | 444.1 |
| 572 |  | 0.312 | 101 | 20 | 32.0 | 1.980 | 300 | 618.4 |
| 573 |  | 0.312 | 101 | 20 | 32.0 | 1.980 | 400 | 859.4 |
| 574 |  | 1.048 | 101 | 20 | 47.0 | 2.080 | 100 | 374.6 |
| 575 |  | 1.048 | 101 | 20 | 47.0 | 2.080 | 200 | 578.2 |
| 576 |  | 1.048 | 101 | 20 | 47.0 | 2.080 | 300 | 933.7 |
| 577 |  | 1.048 | 101 | 20 | 47.0 | 2.080 | 400 | 1149.9 |
| 578 |  | 3.551 | 101 | 20 | 63.0 | 1.990 | 100 | 438.8 |
| 579 |  | 3.551 | 101 | 20 | 63.0 | 1.990 | 200 | 748.1 |
| 580 |  | 3.551 | 101 | 20 | 63.0 | 1.990 | 300 | 1051.9 |
| 581 |  | 3.551 | 101 | 20 | 63.0 | 1.990 | 400 | 1359.5 |
| 582 |  | 12.113 | 101 | 20 | 79.0 | 1.620 | 100 | 469.3 |
| 583 |  | 12.113 | 101 | 20 | 79.0 | 1.620 | 200 | 832.0 |
| 584 |  | 12.113 | 101 | 20 | 79.0 | 1.620 | 300 | 1152.0 |
| 585 |  | 12.113 | 101 | 20 | 79.0 | 1.620 | 400 | 1425.1 |
| 586 | Bai et al. (2020) | 5.353 | 300 | 60 | 56.1 | 2.021 | 100 | 88.4 |
| 587 |  | 5.353 | 300 | 60 | 56.1 | 2.066 | 200 | 137.1 |
| 588 |  | 5.353 | 300 | 60 | 56.1 | 2.078 | 300 | 158.9 |
| 589 |  | 1.428 | 300 | 60 | 26.1 | 2.021 | 100 | 280.0 |
| 590 |  | 1.428 | 300 | 60 | 26.1 | 2.066 | 200 | 570.5 |
| 591 |  | 1.428 | 300 | 60 | 26.1 | 2.078 | 300 | 648.4 |
| 592 | Hu et al. (2021) | 0.980 | 300 | 60 | 0.0 | 1.633 | 200 | 632.4 |
| 593 |  | 0.980 | 300 | 60 | 0.0 | 1.633 | 400 | 1279.4 |
| 594 |  | 0.980 | 300 | 60 | 0.0 | 1.633 | 600 | 1742.4 |
| 595 |  | 0.980 | 300 | 60 | 0.0 | 1.633 | 800 | 2107.8 |
| 596 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 200 | 772.2 |
| 597 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 400 | 1425.7 |
| 598 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 600 | 2000.0 |
| 599 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 800 | 2554.5 |
| 600 | Jin et al. (2017) | 4.920 | 300 | 60 | 0.0 | 2.161 | 100 | 2470.6 |
| 601 |  | 4.920 | 300 | 60 | 0.0 | 2.161 | 200 | 2722.9 |
| 602 |  | 4.920 | 300 | 60 | 0.0 | 2.161 | 300 | 3161.3 |
| 603 |  | 12.680 | 300 | 60 | 40.0 | 2.176 | 100 | 2019.0 |
| 604 |  | 12.680 | 300 | 60 | 40.0 | 2.176 | 200 | 2450.6 |
| 605 |  | 12.680 | 300 | 60 | 40.0 | 2.176 | 300 | 2942.1 |
| 606 |  | 25.640 | 300 | 60 | 70.0 | 2.066 | 100 | 987.9 |
| 607 |  | 25.640 | 300 | 60 | 70.0 | 2.066 | 200 | 1386.3 |
| 608 |  | 25.640 | 300 | 60 | 70.0 | 2.066 | 300 | 1950.8 |
| 609 | Li et al. (2021) | 0.820 | 39.1 | 7.5 | 0.0 | 1.870 | 50 | 175.0 |
| 610 |  | 0.820 | 39.1 | 7.5 | 0.0 | 1.870 | 100 | 224.0 |
| 611 |  | 0.820 | 39.1 | 7.5 | 0.0 | 1.870 | 200 | 297.0 |
| 612 |  | 1.350 | 39.1 | 7.5 | 10.0 | 1.870 | 50 | 179.0 |
| 613 |  | 1.350 | 39.1 | 7.5 | 10.0 | 1.870 | 100 | 234.0 |
| 614 |  | 1.350 | 39.1 | 7.5 | 10.0 | 1.870 | 200 | 316.0 |
| 615 |  | 1.800 | 39.1 | 7.5 | 20.0 | 1.870 | 50 | 189.0 |
| 616 |  | 1.800 | 39.1 | 7.5 | 20.0 | 1.870 | 100 | 246.0 |
| 617 |  | 1.800 | 39.1 | 7.5 | 20.0 | 1.870 | 200 | 346.0 |
| 618 |  | 2.250 | 39.1 | 7.5 | 30.0 | 1.870 | 50 | 196.0 |
| 619 |  | 2.250 | 39.1 | 7.5 | 30.0 | 1.870 | 100 | 254.0 |
| 620 |  | 2.250 | 39.1 | 7.5 | 30.0 | 1.870 | 200 | 369.0 |
| 621 |  | 2.990 | 39.1 | 7.5 | 40.0 | 1.870 | 50 | 207.0 |
| 622 |  | 2.990 | 39.1 | 7.5 | 40.0 | 1.870 | 100 | 266.0 |
| 623 |  | 2.990 | 39.1 | 7.5 | 40.0 | 1.870 | 200 | 406.0 |
| 624 |  | 3.590 | 39.1 | 7.5 | 50.0 | 1.870 | 50 | 223.0 |
| 625 |  | 3.590 | 39.1 | 7.5 | 50.0 | 1.870 | 100 | 300.0 |
| 626 |  | 3.590 | 39.1 | 7.5 | 50.0 | 1.870 | 200 | 474.0 |
| 627 |  | 4.490 | 39.1 | 7.5 | 60.0 | 1.870 | 50 | 238.0 |
| 628 |  | 4.490 | 39.1 | 7.5 | 60.0 | 1.870 | 100 | 357.0 |
| 629 |  | 4.490 | 39.1 | 7.5 | 60.0 | 1.870 | 200 | 551.0 |
| 630 |  | 5.390 | 39.1 | 7.5 | 65.0 | 1.870 | 50 | 246.0 |
| 631 |  | 5.390 | 39.1 | 7.5 | 65.0 | 1.870 | 100 | 375.0 |
| 632 |  | 5.390 | 39.1 | 7.5 | 65.0 | 1.870 | 200 | 594.0 |
| 633 |  | 2.620 | 39.1 | 7.5 | 50.0 | 1.870 | 50 | 231.0 |
| 634 |  | 2.620 | 39.1 | 7.5 | 50.0 | 1.870 | 100 | 315.0 |
| 635 |  | 2.620 | 39.1 | 7.5 | 50.0 | 1.870 | 200 | 472.0 |
| 636 |  | 2.350 | 39.1 | 7.5 | 50.0 | 1.870 | 50 | 236.0 |
| 637 |  | 2.350 | 39.1 | 7.5 | 50.0 | 1.870 | 100 | 326.0 |
| 638 |  | 2.350 | 39.1 | 7.5 | 50.0 | 1.870 | 200 | 498.0 |
| 639 |  | 2.140 | 39.1 | 7.5 | 50.0 | 1.870 | 50 | 244.0 |
| 640 |  | 2.140 | 39.1 | 7.5 | 50.0 | 1.870 | 100 | 334.0 |
| 641 |  | 2.140 | 39.1 | 7.5 | 50.0 | 1.870 | 200 | 528.0 |
| 642 |  | 2.000 | 39.1 | 7.5 | 50.0 | 1.870 | 50 | 251.0 |
| 643 |  | 2.000 | 39.1 | 7.5 | 50.0 | 1.870 | 100 | 344.0 |
| 644 |  | 2.000 | 39.1 | 7.5 | 50.0 | 1.870 | 200 | 553.0 |
| 645 |  | 2.240 | 39.1 | 7.5 | 50.0 | 1.870 | 50 | 242.0 |
| 646 |  | 2.240 | 39.1 | 7.5 | 50.0 | 1.870 | 100 | 326.0 |
| 647 |  | 2.240 | 39.1 | 7.5 | 50.0 | 1.870 | 200 | 518.0 |
| 648 | Zhang et al. (2016) | 2.500 | 292 | 60 | 30.0 | 1.730 | 300 | 903.4 |
| 649 |  | 2.500 | 292 | 60 | 30.0 | 1.730 | 600 | 1774.7 |
| 650 |  | 2.500 | 292 | 60 | 30.0 | 1.730 | 900 | 2565.3 |
| 651 |  | 2.500 | 292 | 60 | 30.0 | 1.730 | 1200 | 3402.0 |
| 652 |  | 4.760 | 292 | 60 | 50.0 | 1.730 | 300 | 1103.6 |
| 653 |  | 4.760 | 292 | 60 | 50.0 | 1.730 | 600 | 1957.1 |
| 654 |  | 4.760 | 292 | 60 | 50.0 | 1.730 | 900 | 2821.3 |
| 655 |  | 4.760 | 292 | 60 | 50.0 | 1.730 | 1200 | 3856.3 |
| 656 |  | 12.110 | 292 | 60 | 79.1 | 1.730 | 300 | 1347.6 |
| 657 |  | 12.110 | 292 | 60 | 79.1 | 1.730 | 600 | 2184.1 |
| 658 |  | 12.110 | 292 | 60 | 79.1 | 1.730 | 900 | 3307.4 |
| 659 |  | 12.110 | 292 | 60 | 79.1 | 1.730 | 1200 | 4086.2 |
| 660 |  | 5.260 | 150 | 60 | 50.0 | 1.730 | 100 | 636.4 |
| 661 |  | 5.260 | 150 | 60 | 50.0 | 1.730 | 300 | 1385.8 |
| 662 |  | 5.260 | 150 | 60 | 50.0 | 1.730 | 600 | 2872.7 |
| 663 |  | 5.260 | 150 | 60 | 50.0 | 1.730 | 900 | 3807.9 |
| 664 |  | 3.700 | 150 | 30 | 50.0 | 1.730 | 100 | 562.0 |
| 665 |  | 3.700 | 150 | 30 | 50.0 | 1.730 | 300 | 1211.8 |
| 666 |  | 3.700 | 150 | 30 | 50.0 | 1.730 | 600 | 1910.7 |
| 667 |  | 3.700 | 150 | 30 | 50.0 | 1.730 | 900 | 2773.1 |
| 668 |  | 3.450 | 150 | 30 | 50.0 | 1.730 | 100 | 463.9 |
| 669 |  | 3.450 | 150 | 30 | 50.0 | 1.730 | 300 | 1124.1 |
| 670 |  | 3.450 | 150 | 30 | 50.0 | 1.730 | 600 | 2093.5 |
| 671 |  | 3.450 | 150 | 30 | 50.0 | 1.730 | 900 | 2709.1 |
| 672 |  | 0.990 | 150 | 30 | 0.0 | 1.730 | 100 | 336.0 |
| 673 |  | 0.990 | 150 | 30 | 0.0 | 1.730 | 300 | 904.0 |
| 674 |  | 0.990 | 150 | 30 | 0.0 | 1.730 | 600 | 1546.4 |
| 675 |  | 0.990 | 150 | 30 | 0.0 | 1.730 | 900 | 2260.1 |
| 676 |  | 6.760 | 292 | 60 | 50.0 | 1.730 | 300 | 1260.0 |
| 677 |  | 6.760 | 292 | 60 | 50.0 | 1.730 | 600 | 2200.0 |
| 678 |  | 3.330 | 150 | 30 | 50.0 | 1.730 | 300 | 1350.0 |
| 679 |  | 3.330 | 150 | 30 | 50.0 | 1.730 | 600 | 2896.0 |
| 680 |  | 3.670 | 101 | 20 | 50.0 | 1.730 | 300 | 1448.0 |
| 681 |  | 3.670 | 101 | 20 | 50.0 | 1.730 | 600 | 3343.0 |
| 682 | Chen (2010) | 18.480 | 300 | 60 | 47.6 | 1.880 | 100 | 805.8 |
| 683 |  | 18.480 | 300 | 60 | 47.6 | 1.880 | 200 | 1102.4 |
| 684 |  | 18.480 | 300 | 60 | 47.6 | 1.880 | 400 | 1467.0 |
| 685 |  | 18.480 | 300 | 60 | 47.6 | 1.880 | 800 | 2076.3 |
| 686 | Chen et al. (2025) | 0.700 | 50 | 8.3 | 20.0 | 2.120 | 100 | 250.0 |
| 687 |  | 0.700 | 50 | 8.3 | 20.0 | 2.120 | 150 | 325.0 |
| 688 |  | 0.700 | 50 | 8.3 | 20.0 | 2.120 | 200 | 400.0 |
| 689 |  | 0.700 | 50 | 8.3 | 20.0 | 2.120 | 250 | 470.0 |
| 690 |  | 0.700 | 50 | 8.3 | 20.0 | 2.120 | 300 | 535.0 |
| 691 |  | 0.870 | 50 | 8.3 | 30.0 | 2.190 | 100 | 292.1 |
| 692 |  | 0.870 | 50 | 8.3 | 30.0 | 2.190 | 150 | 358.4 |
| 693 |  | 0.870 | 50 | 8.3 | 30.0 | 2.190 | 200 | 427.6 |
| 694 |  | 0.870 | 50 | 8.3 | 30.0 | 2.190 | 250 | 503.2 |
| 695 |  | 0.870 | 50 | 8.3 | 30.0 | 2.190 | 300 | 582.4 |
| 696 |  | 1.220 | 50 | 8.3 | 40.0 | 2.210 | 100 | 350.0 |
| 697 |  | 1.220 | 50 | 8.3 | 40.0 | 2.210 | 150 | 420.0 |
| 698 |  | 1.220 | 50 | 8.3 | 40.0 | 2.210 | 200 | 495.0 |
| 699 |  | 1.220 | 50 | 8.3 | 40.0 | 2.210 | 250 | 560.0 |
| 700 |  | 1.220 | 50 | 8.3 | 40.0 | 2.210 | 300 | 620.0 |
| 701 |  | 1.680 | 50 | 8.3 | 50.0 | 2.240 | 100 | 450.0 |
| 702 |  | 1.680 | 50 | 8.3 | 50.0 | 2.240 | 150 | 515.0 |
| 703 |  | 1.680 | 50 | 8.3 | 50.0 | 2.240 | 200 | 585.0 |
| 704 |  | 1.680 | 50 | 8.3 | 50.0 | 2.240 | 250 | 645.0 |
| 705 |  | 1.680 | 50 | 8.3 | 50.0 | 2.240 | 300 | 708.0 |
| 706 |  | 2.800 | 50 | 8.3 | 60.0 | 2.320 | 100 | 482.5 |
| 707 |  | 2.800 | 50 | 8.3 | 60.0 | 2.320 | 150 | 564.0 |
| 708 |  | 2.800 | 50 | 8.3 | 60.0 | 2.320 | 200 | 652.5 |
| 709 |  | 2.800 | 50 | 8.3 | 60.0 | 2.320 | 250 | 785.5 |
| 710 |  | 2.800 | 50 | 8.3 | 60.0 | 2.320 | 300 | 905.5 |
| 711 | Xu et al. (2023) | 0.300 | 39.1 | 6 | 25.0 | 2.210 | 100 | 254.8 |
| 712 |  | 0.300 | 39.1 | 6 | 25.0 | 2.210 | 200 | 407.0 |
| 713 |  | 0.300 | 39.1 | 6 | 25.0 | 2.210 | 300 | 539.0 |
| 714 |  | 0.300 | 39.1 | 6 | 25.0 | 2.210 | 400 | 705.2 |
| 715 |  | 0.440 | 39.1 | 6 | 35.0 | 2.230 | 100 | 290.9 |
| 716 |  | 0.440 | 39.1 | 6 | 35.0 | 2.230 | 200 | 428.1 |
| 717 |  | 0.440 | 39.1 | 6 | 35.0 | 2.230 | 300 | 581.5 |
| 718 |  | 0.440 | 39.1 | 6 | 35.0 | 2.230 | 400 | 750.6 |
| 719 |  | 0.650 | 39.1 | 6 | 45.0 | 2.270 | 100 | 350.5 |
| 720 |  | 0.650 | 39.1 | 6 | 45.0 | 2.270 | 200 | 493.2 |
| 721 |  | 0.650 | 39.1 | 6 | 45.0 | 2.270 | 300 | 622.9 |
| 722 |  | 0.650 | 39.1 | 6 | 45.0 | 2.270 | 400 | 817.9 |
| 723 |  | 0.960 | 39.1 | 6 | 55.0 | 2.265 | 100 | 449.6 |
| 724 |  | 0.960 | 39.1 | 6 | 55.0 | 2.265 | 200 | 585.5 |
| 725 |  | 0.960 | 39.1 | 6 | 55.0 | 2.265 | 300 | 707.7 |
| 726 |  | 0.960 | 39.1 | 6 | 55.0 | 2.265 | 400 | 902.7 |
| 727 | Hu et al. (2021) | 0.980 | 300 | 60 | 0.0 | 1.633 | 200 | 437.3 |
| 728 |  | 0.980 | 300 | 60 | 0.0 | 1.633 | 400 | 884.9 |
| 729 |  | 0.980 | 300 | 60 | 0.0 | 1.633 | 600 | 1147.9 |
| 730 |  | 0.980 | 300 | 60 | 0.0 | 1.633 | 800 | 1311.7 |
| 731 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 200 | 566.2 |
| 732 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 400 | 1017.2 |
| 733 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 600 | 1393.5 |
| 734 |  | 5.180 | 300 | 60 | 60.0 | 1.698 | 800 | 1774.3 |
| 735 | Wang et al. (2017) | 2.340 | 300 | 60 | 20.0 | 2.250 | 200 | 413.1 |
| 736 |  | 2.340 | 300 | 60 | 20.0 | 2.250 | 400 | 622.5 |
| 737 |  | 2.340 | 300 | 60 | 20.0 | 2.250 | 600 | 1025.9 |
| 738 |  | 2.340 | 300 | 60 | 20.0 | 2.250 | 800 | 1364.0 |
| 739 |  | 4.130 | 300 | 60 | 40.0 | 2.340 | 200 | 477.1 |
| 740 |  | 4.130 | 300 | 60 | 40.0 | 2.340 | 400 | 871.3 |
| 741 |  | 4.130 | 300 | 60 | 40.0 | 2.340 | 600 | 1302.6 |
| 742 |  | 4.130 | 300 | 60 | 40.0 | 2.340 | 800 | 1623.3 |
| 743 |  | 7.070 | 300 | 60 | 60.0 | 2.450 | 200 | 595.3 |
| 744 |  | 7.070 | 300 | 60 | 60.0 | 2.450 | 400 | 930.3 |
| 745 |  | 7.070 | 300 | 60 | 60.0 | 2.450 | 600 | 1339.8 |
| 746 |  | 7.070 | 300 | 60 | 60.0 | 2.450 | 800 | 1853.2 |
| 747 |  | 12.810 | 300 | 60 | 80.0 | 2.560 | 200 | 652.2 |
| 748 |  | 12.810 | 300 | 60 | 80.0 | 2.560 | 400 | 1155.4 |
| 749 |  | 12.810 | 300 | 60 | 80.0 | 2.560 | 600 | 1742.2 |
| 750 |  | 12.810 | 300 | 60 | 80.0 | 2.560 | 800 | 2368.2 |
| 751 | Du et al. (2014) | 0.420 | 100 | 25 | 0.0 | 1.800 | 200 | 475.3 |
| 752 |  | 0.420 | 100 | 25 | 0.0 | 1.800 | 400 | 641.0 |
| 753 |  | 0.420 | 100 | 25 | 0.0 | 1.800 | 600 | 783.3 |
| 754 |  | 0.420 | 100 | 25 | 0.0 | 1.800 | 800 | 964.7 |
| 755 |  | 0.920 | 100 | 25 | 20.0 | 1.800 | 200 | 543.2 |
| 756 |  | 0.920 | 100 | 25 | 20.0 | 1.800 | 400 | 852.5 |
| 757 |  | 0.920 | 100 | 25 | 20.0 | 1.800 | 600 | 876.7 |
| 758 |  | 0.920 | 100 | 25 | 20.0 | 1.800 | 800 | 1170.6 |
| 759 |  | 1.380 | 100 | 25 | 30.0 | 1.800 | 200 | 583.3 |
| 760 |  | 1.380 | 100 | 25 | 30.0 | 1.800 | 400 | 1066.5 |
| 761 |  | 1.380 | 100 | 25 | 30.0 | 1.800 | 600 | 1030.0 |
| 762 |  | 1.380 | 100 | 25 | 30.0 | 1.800 | 800 | 1278.1 |
| 763 |  | 2.050 | 100 | 25 | 40.0 | 1.800 | 200 | 959.9 |
| 764 |  | 2.050 | 100 | 25 | 40.0 | 1.800 | 400 | 1167.2 |
| 765 |  | 2.050 | 100 | 25 | 40.0 | 1.800 | 600 | 1080.0 |
| 766 |  | 2.050 | 100 | 25 | 40.0 | 1.800 | 800 | 1483.2 |
| 767 | Ding et al. (2012) | 4.200 | 300 | 60 | 31.0 | 2.150 | 400 | 1452.5 |
| 768 |  | 4.200 | 300 | 60 | 31.0 | 2.150 | 800 | 2418.4 |
| 769 |  | 4.200 | 300 | 60 | 31.0 | 2.150 | 1200 | 3613.4 |
| 770 |  | 4.200 | 300 | 60 | 31.0 | 2.150 | 1600 | 4213.8 |
| 771 |  | 5.880 | 300 | 60 | 39.0 | 2.150 | 400 | 1268.3 |
| 772 |  | 5.880 | 300 | 60 | 39.0 | 2.150 | 1600 | 4305.6 |
| 773 |  | 8.060 | 300 | 60 | 49.0 | 2.150 | 400 | 1322.6 |
| 774 |  | 8.060 | 300 | 60 | 49.0 | 2.150 | 1600 | 4328.0 |
| 775 |  | 12.140 | 300 | 60 | 58.0 | 2.150 | 400 | 1375.0 |
| 776 |  | 12.140 | 300 | 60 | 58.0 | 2.150 | 1600 | 4408.6 |
| 777 |  | 18.080 | 300 | 60 | 67.0 | 2.150 | 400 | 1422.2 |
| 778 |  | 18.080 | 300 | 60 | 67.0 | 2.150 | 800 | 2383.8 |
| 779 |  | 18.080 | 300 | 60 | 67.0 | 2.150 | 1200 | 3452.5 |
| 780 |  | 18.080 | 300 | 60 | 67.0 | 2.150 | 1600 | 4421.2 |
| 781 | Zhang et al. (2015) | 17.870 | 300 | 60 | 80.0 | 2.180 | 800 | 3670.0 |
| 782 |  | 17.870 | 300 | 60 | 80.0 | 2.180 | 1600 | 6930.0 |
| 783 |  | 17.870 | 300 | 60 | 80.0 | 2.180 | 3300 | 11170.0 |
| 784 | Yao et al. (2022) | 0.390 | 100 | 30 | 0.0 | 1.890 | 50 | 104.6 |
| 785 |  | 0.390 | 100 | 30 | 0.0 | 1.890 | 100 | 120.4 |
| 786 |  | 0.390 | 100 | 30 | 0.0 | 1.890 | 200 | 181.7 |
| 787 |  | 0.390 | 100 | 30 | 0.0 | 1.890 | 300 | 206.0 |
| 788 |  | 1.440 | 100 | 30 | 30.0 | 1.890 | 50 | 109.5 |
| 789 |  | 1.440 | 100 | 30 | 30.0 | 1.890 | 100 | 151.9 |
| 790 |  | 1.440 | 100 | 30 | 30.0 | 1.890 | 200 | 233.2 |
| 791 |  | 1.440 | 100 | 30 | 30.0 | 1.890 | 300 | 335.7 |
| 792 |  | 3.430 | 100 | 30 | 50.0 | 1.890 | 50 | 126.3 |
| 793 |  | 3.430 | 100 | 30 | 50.0 | 1.890 | 100 | 204.9 |
| 794 |  | 3.430 | 100 | 30 | 50.0 | 1.890 | 200 | 345.3 |
| 795 |  | 3.430 | 100 | 30 | 50.0 | 1.890 | 300 | 513.7 |
| 796 |  | 8.160 | 100 | 30 | 70.0 | 1.890 | 50 | 133.3 |
| 797 |  | 8.160 | 100 | 30 | 70.0 | 1.890 | 100 | 238.3 |
| 798 |  | 8.160 | 100 | 30 | 70.0 | 1.890 | 200 | 414.2 |
| 799 |  | 8.160 | 100 | 30 | 70.0 | 1.890 | 300 | 627.0 |
| 800 | Wang et al. (2013) | 4.580 | 300 | 40 | 55.4 | 2.280 | 200 | 960.3 |
| 801 |  | 4.580 | 300 | 40 | 55.4 | 2.280 | 300 | 1391.6 |
| 802 |  | 4.580 | 300 | 40 | 55.4 | 2.280 | 400 | 1662.7 |
| 803 | Qin et al. (2025) | 1.520 | 100 | 20 | 30.0 | 2.080 | 100 | 272.2 |
| 804 |  | 1.520 | 100 | 20 | 30.0 | 2.080 | 200 | 358.5 |
| 805 |  | 1.520 | 100 | 20 | 30.0 | 2.080 | 300 | 536.7 |
| 806 |  | 1.520 | 150 | 20 | 30.0 | 2.080 | 100 | 161.0 |
| 807 |  | 1.520 | 150 | 20 | 30.0 | 2.080 | 200 | 283.7 |
| 808 |  | 1.520 | 150 | 20 | 30.0 | 2.080 | 300 | 394.9 |
| 809 |  | 1.520 | 300 | 20 | 30.0 | 2.080 | 100 | 134.2 |
| 810 |  | 1.520 | 300 | 20 | 30.0 | 2.080 | 200 | 255.0 |
| 811 |  | 1.520 | 300 | 20 | 30.0 | 2.080 | 300 | 352.7 |
| 812 | Sun et al. (2016) | 0.950 | 300 | 20 | 10.0 | 1.695 | 100 | 182.3 |
| 813 |  | 0.950 | 300 | 20 | 10.0 | 1.695 | 200 | 460.6 |
| 814 |  | 0.950 | 300 | 20 | 10.0 | 1.695 | 300 | 798.7 |
| 815 |  | 0.950 | 300 | 20 | 10.0 | 1.695 | 400 | 868.1 |
| 816 |  | 1.420 | 300 | 20 | 20.0 | 1.695 | 100 | 320.1 |
| 817 |  | 1.420 | 300 | 20 | 20.0 | 1.695 | 200 | 617.1 |
| 818 |  | 1.420 | 300 | 20 | 20.0 | 1.695 | 300 | 649.5 |
| 819 |  | 1.420 | 300 | 20 | 20.0 | 1.695 | 400 | 887.1 |
| 820 |  | 2.060 | 300 | 20 | 30.0 | 1.695 | 100 | 418.3 |
| 821 |  | 2.060 | 300 | 20 | 30.0 | 1.695 | 200 | 700.1 |
| 822 |  | 2.060 | 300 | 20 | 30.0 | 1.695 | 300 | 938.7 |
| 823 |  | 2.060 | 300 | 20 | 30.0 | 1.695 | 400 | 928.3 |
| 824 | Ma et al. (2025) | 1.650 | 61.8 | 12.36 | 42.0 | 1.600 | 100 | 209.7 |
| 825 |  | 1.650 | 61.8 | 12.36 | 42.0 | 1.600 | 200 | 382.1 |
| 826 |  | 1.650 | 61.8 | 12.36 | 42.0 | 1.600 | 300 | 558.0 |
| 827 |  | 1.650 | 61.8 | 12.36 | 42.0 | 1.600 | 400 | 763.7 |
| 828 |  | 1.141 | 61.8 | 12.36 | 32.0 | 1.600 | 100 | 197.4 |
| 829 |  | 1.141 | 61.8 | 12.36 | 32.0 | 1.600 | 200 | 374.4 |
| 830 |  | 1.141 | 61.8 | 12.36 | 32.0 | 1.600 | 300 | 498.3 |
| 831 |  | 1.141 | 61.8 | 12.36 | 32.0 | 1.600 | 400 | 637.7 |
| 832 |  | 1.043 | 61.8 | 12.36 | 27.0 | 1.600 | 100 | 192.3 |
| 833 |  | 1.043 | 61.8 | 12.36 | 27.0 | 1.600 | 200 | 369.2 |
| 834 |  | 1.043 | 61.8 | 12.36 | 27.0 | 1.600 | 300 | 478.3 |
| 835 |  | 1.043 | 61.8 | 12.36 | 27.0 | 1.600 | 400 | 611.1 |
| 836 |  | 2.388 | 61.8 | 12.36 | 53.0 | 1.600 | 100 | 207.7 |
| 837 |  | 2.388 | 61.8 | 12.36 | 53.0 | 1.600 | 200 | 444.2 |
| 838 |  | 2.388 | 61.8 | 12.36 | 53.0 | 1.600 | 300 | 620.9 |
| 839 |  | 2.388 | 61.8 | 12.36 | 53.0 | 1.600 | 400 | 823.7 |
| 840 | Pei et al. (2025) | 1.248 | 300 | 60 | 10.0 | 1.720 | 100 | 230.0 |
| 841 |  | 1.248 | 300 | 60 | 10.0 | 1.720 | 200 | 508.5 |
| 842 |  | 1.248 | 300 | 60 | 10.0 | 1.720 | 300 | 820.3 |
| 843 |  | 2.621 | 300 | 60 | 30.0 | 2.010 | 100 | 415.9 |
| 844 |  | 2.621 | 300 | 60 | 30.0 | 2.010 | 200 | 781.3 |
| 845 |  | 2.621 | 300 | 60 | 30.0 | 2.010 | 300 | 1192.9 |
| 846 |  | 5.516 | 300 | 60 | 50.0 | 2.090 | 100 | 615.6 |
| 847 |  | 5.516 | 300 | 60 | 50.0 | 2.090 | 200 | 910.4 |
| 848 |  | 5.516 | 300 | 60 | 50.0 | 2.090 | 300 | 1291.4 |
| 849 |  | 11.803 | 300 | 60 | 70.0 | 1.900 | 100 | 534.5 |
| 850 |  | 11.803 | 300 | 60 | 70.0 | 1.900 | 200 | 821.0 |
| 851 |  | 11.803 | 300 | 60 | 70.0 | 1.900 | 300 | 1201.5 |
| 852 |  | 24.763 | 300 | 60 | 90.0 | 1.630 | 100 | 388.9 |
| 853 |  | 24.763 | 300 | 60 | 90.0 | 1.630 | 200 | 743.4 |
| 854 |  | 24.763 | 300 | 60 | 90.0 | 1.630 | 300 | 1264.3 |
| 855 | Zhang et al. (2025) | 12.047 | 300 | 60 | 70.0 | 1.210 | 200 | 797.0 |
| 856 |  | 12.047 | 300 | 60 | 70.0 | 1.210 | 400 | 1237.0 |
| 857 |  | 12.047 | 300 | 60 | 70.0 | 1.210 | 600 | 1873.9 |
| 858 |  | 12.047 | 300 | 60 | 70.0 | 1.210 | 800 | 2306.8 |
| 859 |  | 8.546 | 300 | 60 | 70.0 | 1.210 | 200 | 750.4 |
| 860 |  | 8.546 | 300 | 60 | 70.0 | 1.210 | 400 | 1212.0 |
| 861 |  | 8.546 | 300 | 60 | 70.0 | 1.210 | 600 | 1709.3 |
| 862 |  | 8.546 | 300 | 60 | 70.0 | 1.210 | 800 | 2217.4 |
| 863 |  | 18.590 | 300 | 60 | 70.0 | 1.210 | 200 | 711.1 |
| 864 |  | 18.590 | 300 | 60 | 70.0 | 1.210 | 400 | 1165.5 |
| 865 |  | 18.590 | 300 | 60 | 70.0 | 1.210 | 600 | 1598.4 |
| 866 |  | 18.590 | 300 | 60 | 70.0 | 1.210 | 800 | 2031.3 |
| 867 |  | 10.848 | 300 | 60 | 70.0 | 1.210 | 200 | 646.7 |
| 868 |  | 10.848 | 300 | 60 | 70.0 | 1.210 | 400 | 1144.0 |
| 869 |  | 10.848 | 300 | 60 | 70.0 | 1.210 | 600 | 1530.4 |
| 870 |  | 10.848 | 300 | 60 | 70.0 | 1.210 | 800 | 1888.2 |
| 871 | Zhang et al. (2024) | 8.154 | 300 | 60 | 70.0 | 1.210 | 200 | 561.8 |
| 872 |  | 8.154 | 300 | 60 | 70.0 | 1.210 | 400 | 846.2 |
| 873 |  | 8.154 | 300 | 60 | 70.0 | 1.210 | 600 | 1164.1 |
| 874 |  | 8.154 | 300 | 60 | 70.0 | 1.210 | 800 | 1454.2 |
| 875 |  | 8.782 | 300 | 60 | 70.0 | 1.210 | 200 | 584.1 |
| 876 |  | 8.782 | 300 | 60 | 70.0 | 1.210 | 400 | 1041.4 |
| 877 |  | 8.782 | 300 | 60 | 70.0 | 1.210 | 600 | 1325.9 |
| 878 |  | 8.782 | 300 | 60 | 70.0 | 1.210 | 800 | 1666.1 |
| 879 |  | 9.744 | 300 | 60 | 70.0 | 1.210 | 200 | 506.0 |
| 880 |  | 9.744 | 300 | 60 | 70.0 | 1.210 | 400 | 779.3 |
| 881 |  | 9.744 | 300 | 60 | 70.0 | 1.210 | 600 | 1069.3 |
| 882 |  | 9.744 | 300 | 60 | 70.0 | 1.210 | 800 | 1298.0 |
| 883 |  | 10.176 | 300 | 60 | 70.0 | 1.210 | 200 | 522.7 |
| 884 |  | 10.176 | 300 | 60 | 70.0 | 1.210 | 400 | 757.0 |
| 885 |  | 10.176 | 300 | 60 | 70.0 | 1.210 | 600 | 957.8 |
| 886 |  | 10.176 | 300 | 60 | 70.0 | 1.210 | 800 | 1141.8 |
| 887 |  | 8.735 | 300 | 60 | 70.0 | 1.210 | 200 | 450.4 |
| 888 |  | 8.735 | 300 | 60 | 70.0 | 1.210 | 400 | 702.4 |
| 889 |  | 8.735 | 300 | 60 | 70.0 | 1.210 | 600 | 954.4 |
| 890 |  | 8.735 | 300 | 60 | 70.0 | 1.210 | 800 | 1279.2 |
| 891 |  | 9.807 | 300 | 60 | 70.0 | 1.210 | 200 | 512.0 |
| 892 |  | 9.807 | 300 | 60 | 70.0 | 1.210 | 400 | 915.2 |
| 893 |  | 9.807 | 300 | 60 | 70.0 | 1.210 | 600 | 1296.0 |
| 894 |  | 9.807 | 300 | 60 | 70.0 | 1.210 | 800 | 1626.4 |
| 895 |  | 11.251 | 300 | 60 | 70.0 | 1.210 | 200 | 540.0 |
| 896 |  | 11.251 | 300 | 60 | 70.0 | 1.210 | 400 | 971.2 |
| 897 |  | 11.251 | 300 | 60 | 70.0 | 1.210 | 600 | 1318.4 |
| 898 |  | 11.251 | 300 | 60 | 70.0 | 1.210 | 800 | 1637.6 |
| 899 |  | 12.948 | 300 | 60 | 70.0 | 1.210 | 200 | 624.0 |
| 900 |  | 12.948 | 300 | 60 | 70.0 | 1.210 | 400 | 1066.4 |
| 901 |  | 12.948 | 300 | 60 | 70.0 | 1.210 | 600 | 1340.8 |
| 902 |  | 12.948 | 300 | 60 | 70.0 | 1.210 | 800 | 1676.8 |
| 903 | Dai et al. (2024) | 3.083 | 150 | 30 | 40.0 | 1.980 | 200 | 347.9 |
| 904 |  | 3.083 | 150 | 30 | 40.0 | 1.980 | 400 | 506.1 |
| 905 |  | 3.083 | 150 | 30 | 40.0 | 1.980 | 600 | 802.3 |
| 906 |  | 4.171 | 150 | 30 | 50.0 | 2.040 | 200 | 511.0 |
| 907 |  | 4.171 | 150 | 30 | 50.0 | 2.040 | 400 | 623.4 |
| 908 |  | 4.171 | 150 | 30 | 50.0 | 2.040 | 600 | 1005.8 |
| 909 |  | 5.405 | 150 | 30 | 60.0 | 2.110 | 200 | 620.2 |
| 910 |  | 5.405 | 150 | 30 | 60.0 | 2.110 | 400 | 1071.3 |
| 911 |  | 5.405 | 150 | 30 | 60.0 | 2.110 | 600 | 1438.2 |
| 912 |  | 7.159 | 150 | 30 | 70.0 | 1.940 | 200 | 658.7 |
| 913 |  | 7.159 | 150 | 30 | 70.0 | 1.940 | 400 | 1207.4 |
| 914 |  | 7.159 | 150 | 30 | 70.0 | 1.940 | 600 | 1773.0 |
| 915 |  | 9.665 | 150 | 30 | 80.0 | 1.880 | 200 | 754.5 |
| 916 |  | 9.665 | 150 | 30 | 80.0 | 1.880 | 400 | 1276.3 |
| 917 |  | 9.665 | 150 | 30 | 80.0 | 1.880 | 600 | 1966.4 |
| 918 | Li et al. (2023) | 5.438 | 300 | 60 | 34.7 | 2.050 | 300 | 715.8 |
| 919 |  | 5.438 | 300 | 60 | 34.7 | 2.050 | 600 | 1295.5 |
| 920 |  | 5.438 | 300 | 60 | 34.7 | 2.050 | 900 | 1840.7 |
| 921 | Huang et al. (2015) | 2.575 | 300 | 60 | 25.0 | 2.040 | 200 | 491.5 |
| 922 |  | 2.575 | 300 | 60 | 25.0 | 2.040 | 400 | 918.8 |
| 923 |  | 2.575 | 300 | 60 | 25.0 | 2.040 | 600 | 1397.4 |
| 924 |  | 2.575 | 300 | 60 | 25.0 | 2.040 | 800 | 1859.0 |
| 925 |  | 3.888 | 300 | 60 | 40.0 | 2.140 | 200 | 633.2 |
| 926 |  | 3.888 | 300 | 60 | 40.0 | 2.140 | 400 | 1157.2 |
| 927 |  | 3.888 | 300 | 60 | 40.0 | 2.140 | 600 | 1746.7 |
| 928 |  | 3.888 | 300 | 60 | 40.0 | 2.140 | 800 | 2326.2 |
| 929 |  | 6.109 | 300 | 60 | 55.0 | 2.210 | 200 | 1006.4 |
| 930 |  | 6.109 | 300 | 60 | 55.0 | 2.210 | 400 | 1893.4 |
| 931 |  | 6.109 | 300 | 60 | 55.0 | 2.210 | 600 | 2831.6 |
| 932 |  | 6.109 | 300 | 60 | 55.0 | 2.210 | 800 | 3838.0 |
| 933 | Deng et al. (2013) | 1.916 | 101 | 20 | 20.0 | 1.800 | 100 | 131.5 |
| 934 |  | 1.916 | 101 | 20 | 20.0 | 1.800 | 200 | 245.2 |
| 935 |  | 1.916 | 101 | 20 | 20.0 | 1.800 | 300 | 329.1 |
| 936 |  | 1.916 | 101 | 20 | 20.0 | 1.800 | 400 | 406.5 |
| 937 |  | 1.916 | 101 | 20 | 20.0 | 1.900 | 100 | 125.9 |
| 938 |  | 1.916 | 101 | 20 | 20.0 | 1.900 | 200 | 229.4 |
| 939 |  | 1.916 | 101 | 20 | 20.0 | 1.900 | 300 | 318.5 |
| 940 |  | 1.916 | 101 | 20 | 20.0 | 1.900 | 400 | 401.2 |
| 941 |  | 1.916 | 101 | 20 | 20.0 | 2.000 | 100 | 140.0 |
| 942 |  | 1.916 | 101 | 20 | 20.0 | 2.000 | 200 | 228.0 |
| 943 |  | 1.916 | 101 | 20 | 20.0 | 2.000 | 300 | 334.7 |
| 944 |  | 1.916 | 101 | 20 | 20.0 | 2.000 | 400 | 401.2 |
| 945 |  | 1.916 | 101 | 20 | 20.0 | 2.100 | 100 | 164.0 |
| 946 |  | 1.916 | 101 | 20 | 20.0 | 2.100 | 200 | 270.0 |
| 947 |  | 1.916 | 101 | 20 | 20.0 | 2.100 | 300 | 387.0 |
| 948 |  | 1.916 | 101 | 20 | 20.0 | 2.100 | 400 | 441.0 |
| 949 |  | 3.281 | 101 | 20 | 20.0 | 1.900 | 100 | 140.6 |
| 950 |  | 3.281 | 101 | 20 | 20.0 | 1.900 | 200 | 250.5 |
| 951 |  | 3.281 | 101 | 20 | 20.0 | 1.900 | 300 | 316.9 |
| 952 |  | 2.729 | 101 | 20 | 20.0 | 1.900 | 100 | 144.4 |
| 953 |  | 2.729 | 101 | 20 | 20.0 | 1.900 | 200 | 243.8 |
| 954 |  | 2.729 | 101 | 20 | 20.0 | 1.900 | 300 | 343.9 |
| 955 |  | 2.729 | 101 | 20 | 20.0 | 1.900 | 400 | 406.4 |
| 956 |  | 1.415 | 101 | 20 | 20.0 | 1.900 | 100 | 125.1 |
| 957 |  | 1.415 | 101 | 20 | 20.0 | 1.900 | 200 | 216.5 |
| 958 |  | 1.415 | 101 | 20 | 20.0 | 1.900 | 300 | 321.4 |
| 959 |  | 1.415 | 101 | 20 | 20.0 | 1.900 | 400 | 416.7 |
| 960 |  | 0.945 | 101 | 20 | 20.0 | 1.900 | 100 | 131.1 |
| 961 |  | 0.945 | 101 | 20 | 20.0 | 1.900 | 200 | 216.7 |
| 962 |  | 0.945 | 101 | 20 | 20.0 | 1.900 | 300 | 305.3 |
| 963 |  | 0.945 | 101 | 20 | 20.0 | 1.900 | 400 | 409.9 |
| 964 | Wang et al. (2023) | 0.020 | 101 | 20 | 0.0 | 1.610 | 100 | 187.1 |
| 965 |  | 0.020 | 101 | 20 | 0.0 | 1.610 | 200 | 292.9 |
| 966 |  | 0.020 | 101 | 20 | 0.0 | 1.610 | 300 | 434.1 |
| 967 |  | 0.020 | 101 | 20 | 0.0 | 1.610 | 400 | 561.2 |
| 968 |  | 0.104 | 101 | 20 | 20.0 | 1.860 | 100 | 286.6 |
| 969 |  | 0.104 | 101 | 20 | 20.0 | 1.860 | 200 | 438.4 |
| 970 |  | 0.104 | 101 | 20 | 20.0 | 1.860 | 300 | 593.7 |
| 971 |  | 0.104 | 101 | 20 | 20.0 | 1.860 | 400 | 752.5 |
| 972 |  | 0.341 | 101 | 20 | 40.0 | 1.980 | 100 | 244.9 |
| 973 |  | 0.341 | 101 | 20 | 40.0 | 1.980 | 200 | 446.1 |
| 974 |  | 0.341 | 101 | 20 | 40.0 | 1.980 | 300 | 650.8 |
| 975 |  | 0.341 | 101 | 20 | 40.0 | 1.980 | 400 | 866.1 |
| 976 |  | 1.101 | 101 | 20 | 60.0 | 2.080 | 100 | 372.7 |
| 977 |  | 1.101 | 101 | 20 | 60.0 | 2.080 | 200 | 658.6 |
| 978 |  | 1.101 | 101 | 20 | 60.0 | 2.080 | 300 | 940.9 |
| 979 |  | 1.101 | 101 | 20 | 60.0 | 2.080 | 400 | 1212.7 |
| 980 |  | 3.613 | 101 | 20 | 80.0 | 1.990 | 100 | 436.9 |
| 981 |  | 3.613 | 101 | 20 | 80.0 | 1.990 | 200 | 744.0 |
| 982 |  | 3.613 | 101 | 20 | 80.0 | 1.990 | 300 | 1065.2 |
| 983 |  | 3.613 | 101 | 20 | 80.0 | 1.990 | 400 | 1368.7 |
| 984 |  | 12.035 | 101 | 20 | 100.0 | 1.620 | 100 | 483.5 |
| 985 |  | 12.035 | 101 | 20 | 100.0 | 1.620 | 200 | 836.5 |
| 986 |  | 12.035 | 101 | 20 | 100.0 | 1.620 | 300 | 1154.1 |
| 987 |  | 12.035 | 101 | 20 | 100.0 | 1.620 | 400 | 1489.4 |
| 988 | Zhao et al. (2023) | 2.173 | 100 | 20 | 20.0 | 1.650 | 200 | 544.7 |
| 989 |  | 2.173 | 100 | 20 | 20.0 | 1.650 | 400 | 900.9 |
| 990 |  | 2.173 | 100 | 20 | 20.0 | 1.650 | 550 | 1137.0 |
| 991 |  | 2.173 | 100 | 20 | 20.0 | 1.650 | 700 | 1335.8 |
| 992 |  | 2.983 | 100 | 20 | 30.0 | 1.750 | 200 | 587.9 |
| 993 |  | 2.983 | 100 | 20 | 30.0 | 1.750 | 400 | 955.3 |
| 994 |  | 2.983 | 100 | 20 | 30.0 | 1.750 | 550 | 1187.6 |
| 995 |  | 2.983 | 100 | 20 | 30.0 | 1.750 | 700 | 1460.2 |
| 996 |  | 3.782 | 100 | 20 | 40.0 | 1.850 | 200 | 636.4 |
| 997 |  | 3.782 | 100 | 20 | 40.0 | 1.850 | 400 | 977.3 |
| 998 |  | 3.782 | 100 | 20 | 40.0 | 1.850 | 550 | 1243.2 |
| 999 |  | 3.782 | 100 | 20 | 40.0 | 1.850 | 700 | 1534.1 |
| 1000 |  | 4.970 | 100 | 20 | 50.0 | 1.950 | 200 | 721.0 |
| 1001 |  | 4.970 | 100 | 20 | 50.0 | 1.950 | 400 | 1102.0 |
| 1002 |  | 4.970 | 100 | 20 | 50.0 | 1.950 | 550 | 1375.6 |
| 1003 |  | 4.970 | 100 | 20 | 50.0 | 1.950 | 700 | 1764.2 |

References

Tu Y (2017) The macro and meso mechanical characteristics and nonlinear elastoplastic constitutive model of soil-rock aggregate. Dissertation, Chongqing University, Chongqing.

Li H, Rao X, Jiang J, et al. (2023) Differences in strength properties of soil-rock mixture under simple shear and triaxial compression. Journal of Changjiang River Scientific Research Institute 40(3): 105-111.

Zhang J, Huang H, Mei L, et al. (2023) Triaxial shear tests on soil-rock mixture and 3D multi-shear bounding surface model. Chinese Journal of Geotechnical Engineering 45: 644-651.

Ding F (2023) Research on modification of anti-seepage material of earth-rock dam core by adding gravel. Thesis, Northwest A&F University, Xianyang.

Lv X, Cheng B, Zhang J, et al. (2023) Experimental study on the influence of moisture content on the mechanical properties of soil-rock mixture. Journal of Ground Improvement 5: 97-104.

Tao M, Ren Q, Bian H, Cao M, Jia Y (2022) Mechanical properties of soil-rock mixture filling in fault zone based on mesostructure. Computer Modeling in Engineering & Sciences 132: 681-705.

Jin L, Zeng Y, Zhang S (2017) Large scale triaxial tests on effects of rock block proportion and shape on mechanical properties of cemented soil-rock mixture. Rock and Soil Mechanics 38: 141-149.

Fang L (2023) Particle breakage characteristic of soil-rock mixture in waste slag dam under triaxial test. Thesis, Xi'an University of Technology, Xi'an.

Gao C (2005) The laboratory study of road property and quality appraisal on earth and rock mixture. Thesis, Sichuan University, Chengdu.

Dong H, Peng B, Gao Q, Hu Y, Jiang X (2021) Study of hidden factors affecting the mechanical behavior of soil–rock mixtures based on abstraction idea. Acta Geotech 16: 595-611.

Huang Y, Li J, Ma D, Gao H, Guo Y, Ouyang S (2019) Triaxial compression behaviour of gangue solid wastes under effects of particle size and confining pressure. Sci Total Environ 693: 133607.

Zhang T, Wen Y, Du XZ, et al. (2019) Large-scale Shear Strength Tests of Earth-rock Embankment Material from River Dredging. Journal of Yangtze River Scientific Research Institute 36: 77-80.

Wang Y (2020) The mechanical characteristics of rockfall materials under true triaxial stress conditions. Dissertation, Tsinghua University, Beijing.

Qin S, Chen S, Han Z, Xu X (2010) Large-scale triaxial test study of behavior of over coarse-grained soils. Rock and Soil Mechanics 31: 189-192.

Jiang J, Pan J, Cheng Z, et al. (2018) Large-scale true triaxial tests on strength characteristics of coarse-grained soils. Chinese Journal of Geotechnical Engineering 40: 32-36.

Yang Y (2022) Triaxial test research on mechanical properties of poor sand-gravel material for overburden foundation. Thesis, Xi'an University of Technology, Xi'an.

Lv X, Yan Y, Ma Y, Zhang P (2022) Study on large scale triaxial test on the static characteristics of coarse grained soil filling for high-speed railway subgrade. Subgrade Engineering 1: 39-43.

Ma Y, Jiang J (2021) Study on mechanical properties of gravel tailings dam by large-scale triaxial shear test. China Mine Engineering 50: 5-8.

Wang L (2022) Study on mechanical properties and scale effect analysis of coarse-grained material for dam construction. Thesis, North China University of Water Resources and Electric Power, Zhengzhou.

Tian S, Lu F, Lian P, Ling S (2019) Influence analysis of coarse grain content on macro-mechanical properties of sandy pebbles. Science Technology and Engineering 19: 186-191.

Wang S (2012) Research on mechanical property and constitutive mode of coarse-grained soils. Thesis, Central South University, Changsha.

Jiang JS, Cheng JL, Zuo YZ, Ding HS (2014) Dilatancy of coarse-grained soil in large-scale triaxial tests study. Rock and Soil Mechanics 35: 3129-3138.

Chu F, Zhu J, Wang G, Liu H (2011) Large-scale triaxial test study on deformation and strength characteristics of coarse grained material. Journal of Shandong Agriculture University (Natural Science) 42: 572-578.

Shi X, Zhang J, Meng F, et al. (2014) Large-scale triaxial test of reinforced coarse-grained soils. Journal of Sichuan University (Engineering Science Edition) 46: 52-58.

Chen X (2010) Study of dilatancy effect of redstone coarse grained soil by large scale triaxial tests. Chinese Journal of Rock Mechanics and Engineering 29: 3145-3149.

Wang Y, Pan J, Zhang H, Zhou S, Xu H (2023) Study on the strength and deformation characteristics of coarse-grained soil under end-restraint and end-free (Microfriction) Conditions. Appl Sci 13: 11521.

Chu F (2014) Influence Factor on Dilatancy of Coarse-Grained Soil Based on Large-Scale Triaxial Test. Advanced Materials Research 919-921: 687-692.

Zhao H, He C, Wang C, et al. (2008) Research on tangent modulus of gravel core materials under high pressure. Rock and Soil Mechanics 29(S1):193-196.

Han SL (2010) The research of the K-G model about the material properties of Lianghekou high earth rock-fill dam and dam computation analyzes. Thesis, Sichuan University, Chengdu.

Lian YH (2010) Size effects of coarse-grained materials in triaxial test. Thesis, Sichuan University, Chengdu.

Asghari E, Toll DG, Haeri SM (2003) Triaxial behaviour of a cemented gravely sand, Tehran alluvium. Geotechnical and Geological Engineering 21: 1-28.

Xu W, Zhang H (2021) Research on the effect of rock content and sample size on the strength behavior of soil-rock mixture. Bull Eng Geol Environ 80: 2715-2726.

Zhang H, Xu W, Yu Y (2016) Triaxial tests of soil–rock mixtures with different rock block distributions. Soils and Foundations 56: 44-56.

Zhao Y, Liu Z (2018) Study of material composition effects on the mechanical properties of soil-rock mixtures. Adv Civ Eng 1-10.

Zhao Y, Liu Z (2019) Numerical experiments on triaxial compression strength of soil-rock mixture. Adv Civ Eng 1-15.

Chen S, Zhao M, Wang K (2023) Analysis of electrical resistivity characteristics of soil-rock mixture under triaxial condition. Chinese Journal of Underground Space and Engineering 19: 1859-1869,1906.

Tan C, Wu Y, Wan L, et al. (2015) Size effects on the shear strength of the cohesionless coarse-grained soils under the triaxial compression condition. Journal of Jiangnan University (Natural Science Edition) 14: 810-813.

Wan H, Zhou Y, Deng M, et al. (2024) Meso-evolution of shear band of coarse-grained soil under triaxial loading. Journal of Hydroelectric Engineering 1-10.

Wang X, Chen X, Wang C (2023) Study on strength properties of soil-rock mixtures with different gravel content. Sichuan Water Resources 44(1):19-21.

Bai Y, Wang Y, Huang R (2020) Meso-structural characteristics and failure process of a soil-rock mixture landslide in a deeply incised valley. Thesis, Chengdu University of Technology. https://doi.org/10.26986/d.cnki.gcdlc.2020.000207

Hu S, Jin X, Sun G, Li H, Nie Z (2021) Large-scale triaxial tests and coupled PFC-FLAC simulation of soil-rock mixture. Chinese Journal of Rock Mechanics and Engineering 40(S2): 3344-3356. https://doi.org/10.13722/j.cnki.jrme.2021.0019

Li C, Hu J (2021) Mechanical properties and slope stability of soil-rock mixture in the Gongchangling open-pit iron mine. Thesis, University of Science and Technology Liaoning. https://doi.org/10.26923/d.cnki.gasgc.2021.000098

Zhang H, Yu Y (2016) Mesostructural mechanics and scale effects of soil-rock mixtures. Thesis, Tsinghua University.

Chen T, Sun W, Feng A (2025) Deformation and failure characteristics of soil-rock mixtures under coupled stress-seepage effects. Thesis, Lanzhou Jiaotong University. https://doi.org/10.27205/d.cnki.gltec.2024.001583

Xu N, Sun W (2023) Macro- and meso-mechanical properties of soil-rock mixtures under seepage. Thesis, Lanzhou Jiaotong University. https://doi.org/10.27205/d.cnki.gltec.2023.001460

Wang P, Liu X, Yi L (2017) Large-scale triaxial tests of soil-rock mixtures and PFC simulation of their mesomechanical characteristics. Thesis, Chongqing University.

Du S, Zhang D (2014) Strength and deformation characteristics of soil-rock mixtures and soil-rock interactions. Thesis, Nanjing University.

Ding X, Zhang H, Huang S, Lu B, Zhang Q (2012) Mechanical properties of unsaturated soil-rock mixtures based on mesoscopic numerical tests. Chinese Journal of Rock Mechanics and Engineering 31(8): 1553-1566.

Zhang Z, Zhang G, Chan D (2015) Mesoscopic numerical simulation of triaxial tests on coarse-grained soil based on PFC3D. Thesis, China Three Gorges University.

Yongsheng Yao, Jue Li, Junjun Ni, Chenghao Liang, Anshun Zhang (2022) Effects of gravel content and shape on shear behaviour of soil-rock mixture: Experiment and DEM modelling. Computers and Geotechnics 141: 104476. https://doi.org/10.1016/j.compgeo.2021.104476

Wang J, Zhang J (2013) Experimental study on dynamic elastic modulus and damping ratio of coarse-grained soil. Thesis, Central South University.

Qin Y, Yuan X, Ma S, Zhang Y (2025) Experimental study of size effects on the static characteristics of soil-rock mixtures. Chinese Journal of Underground Space and Engineering 21(S2): 700-708. https://doi.org/10.20174/j.JUSE.2025.S2.20

Sun W, Song Y, Lu W, Guo K, Sun C (2016) Experimental study on the mechanical properties of loess-crushed stone mixtures. Highway 61(5): 178-181.

Ma Z, Zhang Z, Zhang Y, Chen W, Lu B, Huang B (2025) Shear strength characteristics of soil-rock mixtures in a copper mine waste dump considering gradation effects. Water Resources Planning and Design (11): 135-141.

Pei X, Luo J, Dong Z (2025) Triaxial experimental study on the mechanical properties of TBM tunnel muck considering accumulation structure characteristics. Chinese Journal of Geotechnical Engineering 1-10.

Chao Zhang, Aoqing Lou, Jin Yu, Dongping Zhu, Zan Xu, Wengui Cao (2025) Discontinuous gradation effect on large-scale triaxial shear mechanical properties of soil-rock mixture. Chinese Journal of Rock Mechanics and Engineering 44(5): 1300-1312. https://doi.org/10.3724/1000-6915.jrme.2024.0789

Zhang C, Yu J, Zhu D, Gong J, Li Z (2024) Particle-size gradation effects on the large-scale triaxial shear mechanical properties of soil-rock mixtures. China Journal of Highway and Transport 37(10): 61-72. https://doi.org/10.19721/j.cnki.1001-7372.2024.10.006

Dai X, Song Y, Zhang Z, Qi Z, Liu Q (2024) Mechanical properties and particle breakage of soil-rock mixtures. Journal of Hebei University of Water Resources and Electric Engineering 34(1): 1-8. https://doi.org/10.16046/j.cnki.issn2096-5680.2024.01.001

Huang W, Cao W (2015) Large-scale triaxial tests on soil-rock mixtures based on orthogonal design. Thesis, Hunan University.

Deng W, Wang J (2013) Triaxial tests on the strength and deformation characteristics of sandstone-mudstone mixtures. Thesis, Chongqing Jiaotong University.

Mingjie Zhao, Songlin Chen, Kui Wang, Gang Liu (2023) Analysis of Electrical Resistivity Characteristics and Damage Evolution of Soil–Rock Mixture under Triaxial Shear. Materials 16(10). https://doi.org/10.3390/ma16103698